BSE and TDDFT at work
Claudio Attaccalite
http://abineel.grenoble.cnrs.fr/
CECAM Yambo School 2013 (Lausanne)

---
Optical Absorption: Microscopic View
Direct and indirect interactions between an e-h pair created by a photon
 Summing up all such interaction processes we get:
L(bold r_1 t_1;bold r_2 t_2; bold r_3 t_3; bold r_4 t_4) = L(1,2,3,4)
The equation for L is the Bethe Salpeter Equation. The poles are the neutral excitations.

---
Bethe Salpeter Equation Historical remarks…
First solution of BSE
with dynamical effects: Shindo approximation
JPSJ 29, 278(1970)
Plane-waves implementation
G. Onida et al.
PRL 75, 818 (1995)
First applications in solids:
 W. Hanke and L.J. Sham PRL 33, 582(1974)
 G. Strinati, H.J. Mattausch and W. Hanke
PRL 45, 290 (1980)
1951
1970
1974
1995

---
Feynman's diagrams and
Bethe-Salpeter equation
=
+
-
Intrinsic 4-point equation.
It describes the (coupled) propagation of
two particles, the electron and the hole !
Retardation effects are neglected
W(1,2) = W(bold r_1 , bold r_2) %delta(t_1 ,t_2)
L(1,2,3,4) = L(bold r_1, bold r_2, bold r_3, bold r_4; t − t_0) = L(1,2,3,4, %omega)
L(1234) = L_0(1234)+ {} {} + L_0(1256) [v(57) color red {%delta(56) %delta(78)} −W(56) color red {%delta(57) %delta(68)}] L(7834)
Quasihole and quasielectron
L = L_0 + L_0 [v − W] L

---
Construction of the BSE 1/2
 We expand L in the independent particle basis
L(r_1,r_2,r'_1,r'_2 mline %omega) = sum from { bold k_1, bold k_2, bold k_3, bold k_4 } %phi_{bold k_1} ( bold r_1) %phi_{bold k_2} (bold r_2) L_{bold k_1,bold k_2,bold k_3, bold k_4} %phi_{bold k_3} ( bold r'_1) %phi_{bold k_4} (bold r'_2)
 We start from L0
L_0(r_1,r_2,r'_1,r'_2 mline %omega) = 2 int {{ d %omega' } over {2 %pi} G_0(r_1, r'_2 ; %omega + %omega') G_0(r_2, r'_1 ; %omega')}
where
G_0(r_1, r_2 ; %omega) = sum from{ bold k,i} {{ %phi^{ {} * {} }_{ bold k, i}(r_1) %phi_{bold k, i}(r_2)} over { hbar %omega - %epsilon_{bold k,i} + i %eta sign(%epsilon_{bold k,i} - %epsilon_F)}}
 ...integrating in the frequency we get...
L^0_{bold k_1,bold k_2,bold k'_1, bold k'_2} = %delta_{ bold k_1, bold k_2} %delta_{ bold k'_1, bold k'_2} {2i } over {hbar } { f(%epsilon_{bold k_2}) - f (%epsilon_{bold k'_2}) } over {%epsilon_{bold k'_2} - %epsilon_{bold k_2} + i %delta + hbar %omega }

---
Construction of the BSE 2/2
Time-dependent Hartree term:
H^{TD-harteee}_{ij,kl} = 2 int %phi^e_{ i} ( bold r) %phi^{ {} * {}h}_{j} (bold r) V(bold r-bold r') %phi^{ e}_{k} ( bold r') %phi^{ {} * {} h }_{ l } (bold r')
Screened Exchange Coulomb term:
-
H^{TD-SEX}_{ij,kl} = int %phi^e_{ i} ( bold r) %phi^{ {} * {} h}_{j} (bold r') W(bold r, bold r') %phi^{ e}_{k} ( bold r) %phi^{ {} * {} h }_{ l } (bold r')
...and now let's solve the equation...

---
Bethe-Salpeter equation
(4-points - space and time)
Should we invert the equation for L for each frequency???
L(1,2,3,4) = L(bold r_1, bold r_2, bold r_3, bold r_4; t − t_0) = L(1,2,3,4, %omega)
The frequency term can be separated and an-effective Hamiltonian can be derived without any frequency dependency
We work in transition space...
Original BSE
L = L_0 + L_0 [ v -W ] L
left [ L^{-1}_0 + [ v -W ] right ] = L^{-1}
We solve the inverse Bethe-Salpeter eq., because it is easier
-
+
-
+
-
+
H^{exc}_{(n_1 n_2),(n_3 n_4)} A_{%lambda}^{(n_3 n_4)} = E_{%lambda} A_{%lambda}^{(n_1 n_2)}

---
How to transform the BSE in an eigenvalues problem
Using the definition of L0
That is diagonal in the e/h space

---
We can solve the equation once for all frequency!!!!
...with some linear algebra....

---
Absoprtion spectra and BSE

---
BSE calculation in practice

---
… Some results…
Bruneval et al., PRL 97, 267601 (2006)
Strinati et al., Rivista del Nuovo Cimento 11, 1 (1988)
Albrecht et al., PRL 80, 4510
(1998)
Bruno et al., PRL 98, 036807 (2007)
V. Garbuio et al., PRL 97, 137402 (2006)
Tiago et al., PRB 70, 193204 (2004)

---
Excitons in nanoscale systems
Nanotubes/Nanowires
Frenkel excitons in photosynthesis
Colloidal quantum dots
Excitons in nanoscale systems
Gregory D. Scholes, Garry Rumbles
Nature Materials 5, 683 - 696 (2006)
[Speaker Notes: The yellowing of paper on aging causes major aesthetic damages of cultural heritage. It is due to cellulose oxidation, a complex process with many possible products still to be clarified. By comparing ultraviolet-visible reflectance spectra of ancient and artificially aged modern papers with ab initio time- dependent density functional theory calculations, we identify and estimate the abundance of oxidized functional groups acting as chromophores and responsible of paper yellowing. This knowledge can be used to set up strategies and selective chemical treatments preventing paper yellowing.]

---
BSE for charge transfer excitons
donor-acceptor complexes: benzene, naphthalene, and anthracene derivatives with the tetracyanoethylene acceptor
X. Blase and C. Attaccalite Apl. Phys. Lett. 99, 171909 (2011)

---
Exciton analysis

---
Solving the equations
in a smart way ...

---
R
The BSE can be large...... too large

---
Tamm-Dancoff approximation

---
The dielectric constant doesn't require too much information

---
Let's come back to the original formula
we can write the dielectric constant as
%epsilon_2(%omega, bold q) = 4 %pi Im left[ langle P mline {1} over { %omega - H_{EXC} + i%eta } mline P rangle right]
left none mline P right rangle = lim_{q toward 0} {e^{iqr}} over {q} left none mline 0 right rangle
...and ask the help
of mathematicians...

---
Lanczos-Haydock method

---
Lanczos-Haydock algorithm

---
Lanczos-Haydock performance

---
What about TDDFT?

---
TDDFT versus BSE
BSE
TDDFT
BSE is a 4-points equation => unavoidable
TDDFT is a 2-points equation => that can be rewritten as a 4-point equation
L(1234) = L_0(1234)+ {} {} + L_0(1256) [v(57) color red {%delta(56) %delta(78)} −W(56) color red {%delta(57) %delta(68)}] L(7834)
%chi(12) = %chi_0(12) + %chi_0(13) [v(34) + f_{xc}] %chi(42)

---
TDDFT in G-space
Simple static fxc case:
%chi_{bold G,bold {G'}} (bold q, %omega)= %chi^0_{bold G,bold {G'}} (bold q, %omega) + %chi^0_{bold G,bold {G^2}} (bold q, %omega) (v_{G^2}(bold q) + f^{xc}_{ bold G^2, bold G^3} (bold q)) %chi_{bold {G^3},bold {G}} (bold q, %omega)
Microscopic dielectric constant:
%epsilon^{-1}_{bold G,bold {G'}} (bold q, %omega)= %delta_{bold G, bold {G'}} + v_{bold G} ( bold q) %chi_{bold G, bold {G'}} (bold q, %omega)
Macroscopic dielectric constant:
%epsilon^M (bold q, %omega)= { 1} over {%epsilon^{-1}_{bold G =0,bold {G'}=0} (bold q, %omega) }
Advantages: 2-points eq.
Disadvantages: the eqs. Has to be solved for each frequency

---
TDDFT in e/h space
Time-dependent Hartree term:
H^{TD-hartree}_{ij,kl} = 2 int %phi^e_{ i} ( bold r) %phi^{ {} * {}h}_{j} (bold r) V(bold r-bold r') %phi^{ e}_{k} ( bold r') %phi^{ {} * {} h }_{ l } (bold r')
Time-dependent exchange correlation function:
-
f_{xc}(bold r, bold r') = { partial V_{xc} (r) } over { partial %rho(r')}
H^{TD-EXC}_{ij,kl} = int %phi^e_{ i} ( bold r) %phi^{ {} * {}h}_{j} (bold r) f_{xc}(bold r, bold r') %phi^{ e}_{k} ( bold r') %phi^{ {} * {} h }_{ l } (bold r')
BSE
H^{TD-SEX}_{ij,kl} = int %phi^e_{ i} ( bold r) %phi^{ {} * {} h}_{j} (bold r') W(bold r, bold r') %phi^{ e}_{k} ( bold r) %phi^{ {} * {} h }_{ l } (bold r')

---
Beyond the Tamm-Dancoff approx.

---
Tamm-Dancoff breakdown 1

---
Tamm-Dancoff breakdown 2

---
Don't worry!
Haydock method still works

---
SUMMARY
Optical spectra can be calculated by mean of Green's function theory
TDDFT and BSE can efficiently be formulated in the e/h space
By using Lanczos-Haydock approach we do not need to diagonalize the full matrix!
-

---
References!!!
Reviews:
Application of the Green’s functions method to the study of
the optical properties of semiconductors
Nuovo Cimento, vol 11, pg 1, (1988) G. Strinati
Effects of the Electron–Hole Interaction on the Optical Properties
of Materials: the Bethe–Salpeter Equation
Physica Scripta, vol 109, pg 141, (2004) G. Bussi
Electronic excitations: density-functional versus many-body
 Green's-function approaches
RMP, vol 74, pg 601, (2002	) G. Onida, L. Reining, and A. Rubio
Books:
On the web:
http://yambo-code.org/lectures.php
http://freescience.info/manybody.php
http://freescience.info/tddft.php
http://freescience.info/spectroscopy.php