What is the nature of the C-C complex in silicon?
Insights from electronic structure calculations
Claudio Attaccalite
CNRS/CINAM Campus de Luminy, Case 913
13288 Marseille , France

---
Silicon Laser : the problem
Indirect band gap semiconductors are not good for photonics/optoelectronics

---
Silicon Laser : solutions
Defects (G-centers)
Nanostructures
and more…. hybryd lasers etc...

---
Silicon Laser in the news

---
The G-center in Silicon
 D. Berhanuddin, M. Lourenco, C. Jeynes, M. Milosavljević, R. Gwilliam, and K. Homewood, Journal of Applied Physics 112, 103110 (2012).
D. D. Berhanuddin, M. A. Lourenço, R. M. Gwilliam, andK. P. Homewood, Advanced Functional Materials 22, 2709 (2012).

---
The CiCs complex
history
Discovered in ‘60 in irradiated Silicon,
and associated to the G-center emission at 0.97 eV (1280 nm)
Carbon isovalent to S occupies substitutional position Cs
Cs binds carbon interstitials and forms CiCs couple!
Experimental studies by means of: Electron-paramagnetic resonance (EPR), Optical detection of magnetic resonance (ODMR), Deep-level Transition-Spectroscopy (DLTS), Photoluminescence Spectroscopy (PS), Infrared Spectroscopy(IS)

---
How to create G-centers….
Carbon doping of silicon using conventional ion implantation is not feasible due to its low
Carbon solubility.
Solution: amorphization → ion implantation → Annealing
Rotem, E., Shainline, J. M., & Xu, J. M. (2007). Electroluminescence of nanopatterned silicon with carbon implantation and solid phase epitaxial regrowth. Optics express, 15(21), 14099-14106.

---
The suspects
A-form:
the interstitial silicon
is three bounded
C-form:
two carbon atoms are situated in a vacancy and
oriented in (100) direction
B-form:
Si is bounded to two
C atoms
D-form:
is a torsion of
C-form along the C-C bond
axis

---
The suspects

---
First clue: binding energy
Depending on approaching manner of Ci to Cs either A or C can be formed. While A will directly transform to B, as B is more stable and the energetic barrier is very low 0.1 eV, transformation from either A or B to C is less probable as the transformation barrier have been estimated to be as high as 2-3 eV.

---
Second clue: vibrational frequiencies
Good agreement with experiments but lack of measurement above the 1000cm^-1. Measurement of the A and B form are obtained exciting the system with light to make the transition B->A
E. V. Lavrov, L. Hoffmann, and B. Bech Nielsen, Phys. Rev. B 60, 8081 (1999).

---
Third clue: defect concentration
The experimental defect concentration
are extracted from infrared spectra.
(Annealing with different
carbon concentration)
Simulation are based on “kinetic Mass
Action Low” on lattice.
Binding and migration energies from DFT

---
Forth clue: band structure/optics
We started from the DFT-PBE bans structure and corrected it using Many-Body Perturbation Theory (MBPT) within the G0W0 approximation

---
Forth clue: band structure/optics
The optical absortion
is calculated by means of the Bethe-Salpeter equation

---
Who is the murder ?
We think that the responsible for the G-center light emission
is …...

---
Who is the murder ?
We think that the responsible for the G-center light emission
is …..
the C-form of the CiCs complex
but more experiments are needed to clarify different points.
Many clues point to the C-form but:
1) The C-form is magnetic, therefore its EPR response can be out of the experimental range
2) Different form of CiCs complex could be present in the same sample
3) Vibration frequencies above 1000 cm^-1 not measured yet.

---
Acknoledgments
Dilyara Timerkaeva
Damien
Caliste
Brenet
Gilles
Pascal
Pochet
References
D. Timerkaeva, C. Attaccalite, B. Gilles, D. Caliste, P. Pochet, Which is the nature of the C-C complex in silicon? Insights from electronic structure calculations (submitted to PRB)
Brenet, G., Timerkaeva, D., Sgourou, E. N., Londos, C. A., Caliste, D., & Pochet, P. (2015).
An atomistic vision of the Mass Action Law: Prediction of carbon/oxygen defects in silicon. Journal of Applied Physics, 118(12), 125706.

---
Mass Action Law :
carbon/oxygen defects in silicon
Evolution concentration
Constant rates