Density functional theory
in practice 2/2
How to simulate non-periodic systems
(surfaces, molecules, amorphous, etc..)
STM images
Structural optimization

---
How to simulate metals

---
In Ry typical 0.01

---
STM images
Reference: Theory of Scanning Tunneling Microscopy
[https://arxiv.org/abs/1404.0961]

---
See pp.x manual
http://www.quantum-espresso.org/users-manual/input-data-description/

---
More format available: gnuplot, contour.x, plotrho, 2D, gOpenMol, cube

---
xcrysden --xsf AlAs110-1.0.xsf

---
Data Visualization with Xcrysden 1/2
Tools→ Data grid
Set Isolevel

---
STM theory and experiments
T. Leoni et al.

---
Structure optimization

---
The king of structure optimization
Among the highlights are the discovery of the structure of a superhard phase of boron, gamma-B, transparent phase of sodium, new carbon allotrope, stability of MgSiO3 post-perovskite in the Earth's mantle, prediction and synthesis of "forbidden" compounds (e.g., Na3Cl), discovery of helium chemistry, and creation of borophene - a 2D-monolayer of boron atoms, with great promises for future technologies
see wiki for references.
Artem Oganov
https://en.wikipedia.org/wiki/Artem_R._Oganov

---
Why you will not be as successful
as Artem Organov
Energy landscape too complex
Artem Oganov
https://en.wikipedia.org/wiki/Artem_R._Oganov
Use UPEX!!

---
Structural relaxation
 &control
    calculation= ‘relax’,
    prefix='silicon',
    pseudo_dir='./'
    outdir = ‘./',
 /
 &system
    ibrav= 2,
    celldm(1) =10.2,
    nat= 2,
    ntyp= 1,
    ecutwfc = 12.0,
 /
 &electrons
 /
&ions
  ions_dynamics=’damp’ or ‘BFGS’
/
ATOMIC_SPECIES
 Si 28.086 Si.vbc.UPF
ATOMIC_POSITIONS {crystal}
 Si 0.00 0.00 0.00
 Si 0.25 0.25 0.25
K_POINTS automatic
2 2 2 0 0 0
New calculation type
New namelist
Optimization methods for finding minimum energy paths
J. Chem. Phys. 128, 134106 (2008)

---
Input file for the 3x3 graphene: graphene3x3.in
Input file for the oxygen: oxygen.in
Put the oxygen on the graphene and relax the structure
Calculate the absorption energy
E_abs = E_tot – E_graphene -E_o

---
Data Visualization with Xcrysden
Tools→ Data grid
Set Isolevel