Impact of electronic correlation
on electron-phonon coupling
Claudio Attaccalite
Institute Neel, Grenoble (France)
Belfast 27/07/2015

---
Electron-phonon coupling: why?
Superconductivity
Joule's heating
Electron relaxation
(luminescence)
Raman Spectroscopy

---
Electron-phonon coupling: definition
color red {H(x + u)}= H(x) " " + " " {partial H} over {partial x} " " u " " + " " {1} over {2} " " {partial^2 H} over {partial x^2} " " u^2 " " + ...
For every single particle
Hamiltonian
(Kohn-Sham, Tight-binding, etc..)
Second order expansion
LUMO
EPC ~ |slope|2
(3-fold)
Stepwise deformation
Changes in electronic structure
Structural deformation

---
Electron-phonon coupling: how?
DFT is an exact theory for the ground state (atomic structure, phonons, etc..)
EPC matrix elements
can be obtained from the Kohn-Sham eigenstates, but there is no guarantee
that they are good

---
Correction to the band structure
Using Many-body Perturbation Theory we can correct DFT results
%epsilon_{QP} simeq %epsilon_{ KS } + int G( %omega-%omega^{{}, {}} ) W( %omega^{ {} , {} } ) + ...
GW is the first order correction in terms of screened interaction
W( %omega ) = { V_{ ee } } over { %epsilon ( %omega) }
Aryasetiawan, F., & Gunnarsson, O. The GW method. Reports on Progress in Physics, 61(3), 237.(1998).
It works very well!!!

---
...an old story

---
More recently...
RAMAN on graphene 1/2

---
RAMAN in graphene 2/2
→	Double resonant RAMAN
→	D-line dispersion
I. Pócsik et al., J. Non-Cryst. Solids 227, 1083 (1998)
P. H. Tan et al., Phys. Rev. B 66, 245410 (2002).
J. Maultzsch et al., Phys. Rev. B 70, 155403 (2004).
%tendto %omega_q
K
K'
{
q

---
GW correction to the EPC
P_q = {4} over {N_k} sum from{k} { { {abs{D_{(k+q) %pi^{%perthousand},k %pi }}}^{2} } over {%epsilon_{k,%pi}-%epsilon_{k+q,%pi^{%perthousand}}} }
Impact of the electron-electron correlation on phonon dispersion: Failure of LDA and GGA DFT functionals in graphene and graphite
Michele Lazzeri, Claudio Attaccalite, Ludger Wirtz, and Francesco Mauri
Phys. Rev. B 78, 081406(R) (2008)

---
 Phonons dispersion of graphene
Recent Experimental evidences
Phonon dispersions around the K point of graphite by inelastic x-ray scattering
Experimental phonon dispersion in bilayer graphene obtained by Raman spectroscopy
A. Grüneis et al . Phys. Rev. B 80, 085423 (2009)
D. L. Mafra et al. Phys. Rev. B 80, 241414(R)(2009)
langle D^2_K rangle_F = 166 (eV/circle A )
inelastic x-ray
langle D^2_K rangle_F = 164 (eV/circle A )
GW

---
EPC in fullerenes
Electron-phonon potential
ev-GW
LDA 73 meV
evGW 101 meV
Exp. 107 meV
DFT-LDA
LUMO
DFT:	J. Laflamme-Janssen, PRB 2010;
GW:	C. Faber, J. of Mat. S., 47, 7472(2012)
Exp:	Wang, JCP 2005; Hands, PRB 2008;
(3-fold)
Electron–phonon coupling and charge-transfer excitations in organic systems from many-body perturbation theory
C. Faber et al., J. of Material Science, 47, 7472(2012)

---
Bismuthates, Chloronitrides and
other high-Tc superconductors
Correlation-Enhanced Electron-Phonon Coupling: Applications of GW and Screened Hybrid Functional to Bismuthates, Chloronitrides, and Other High-Tc Superconductors
Z. P. Yin, A. Kutepov, and G. Kotliar
Phys. Rev. X 3, 021011 (2013)

---
Bismuthates, Chloronitrides and
other high-Tc superconductors
critical temperature Tc
Correlation-Enhanced Electron-Phonon Coupling: Applications of GW and Screened Hybrid Functional to Bismuthates, Chloronitrides, and Other High-Tc Superconductors
Z. P. Yin, A. Kutepov, and G. Kotliar
Phys. Rev. X 3, 021011 (2013)

---
Diamond gap?
Electron-Phonon Renormalization of the Direct Band Gap of Diamond
Feliciano Giustino, Steven G. Louie, and Marvin L. Cohen
Phys. Rev. Lett. 105, 265501 (2010)
Effect of the Quantum Zero-Point Atomic Motion on the Optical and Electronic Properties of Diamond and Trans-Polyacetylene
Elena Cannuccia and Andrea Marini
Phys. Rev. Lett. 107, 255501(2011)
[Speaker Notes: pernickitiness]

---
GW renormalization of EPC
and diamond gap
Many-Body Effects on the Zero-Point Renormalization of the Band Structure
G. Antonius, S. Poncé, P. Boulanger, M. Côté, and X. Gonze
Phys. Rev. Lett. 112, 215501 (2014)

---
New physics appears...
EPC for the K-A′ phonon aquires a strong doping dependence
Doped graphene as tunable electron-phonon coupling material
C. Attaccalite et al., Nanoletters, 10, 1172(2010)

---
Experimental confirmation
Raman signature of electron-electron correlation in chemically doped few-layer graphene
Phys. Rev. B 83, 241401(R) (2011)
Matteo Bruna and Stefano Borini
Pressure-mediated doping in graphene
Nanoletters, 11, 3564 (2011)
J. Nicolle,D. Machon, P. Poncharal,O. Pierre-Louis
and Alfonso San-Miguel

---
Simplified approach
1) Static screening (COHSEX)
Inspired by the
Bethe-Salpeter
equation
{partial %SIGMA^{GW} } over {partial bold u^{bold q %nu}} simeq { {partial %SIGMA^{COHSEX} } over {partial bold u^{bold q %nu}} }
W ( %omega ) simeq W( 0 )
2) Constant screening respect to
       the phonon displacement
{partial GW} over {partial bold u^{bold q %nu}} simeq left({ {partial G} over {partial bold u^{bold q %nu}} } right ) W

---
The simplified approach works!
Approximation to the GW self-energy
electron-phonon coupling gradients
C. Faber et al.
Physical Review B 91 (15), 155109(2015)

---
Conclusions
1) Electron-phonon coupling from Kohn-Sham
     under/overestimate the real one
2) Many-Body-Perturbation Theory
    can be used to correct the EPC
3) The new EPC matrix elements improve:
     Raman, phonons, band-gap renomalization, Tc
4) New physics can appear!
5) If calculations are too heavy ….
use our simplified approach

---
Acknowledgments
Ivan
Duchemin
Xavier
Blase
Carina
Faber
Paul
Boulanger
Elena
Cannuccia
Alexander
Gruneis
Francesco
Mauri
Angel
Rubio
Ludger
Wirtz
Michele
Lazzeri

---
Bands renormalization
Frozen phonon approach

---
Electron-phonon coupling
→	The frozen-phonon approach:
LUMO
EPC ~ |slope|2
(3-fold)
Stepwise deformation
Changes in electronic structure
Structural deformation

---
Electron-phonon coupling and doping
%lambda_{bold q %nu} = {2} over {hbar %omega_{bold q %nu} N_{%sigma}(%epsilon_{f})} int_{BZ} { {d bold k} over { %OMEGA} sum_{i,j} abs{g^%nu_{bold ki,(bold k + bold q,j)}}^2 %delta(%epsilon_k - %epsilon_k) %delta(%epsilon_{k+q} - %epsilon_f)}
..where the electron-phonon matrix element..
g^%nu_{bold ki,(bold k + bold q,j)} = langle bold k + bold q,j abs{ %DELTA V_{bold q %nu}} bold k,i rangle
describe the scattering of an electron from the band I to band j due to the phonon n
Has been always considered a constant
with respect to the electron/hole doping

---
Diagrammatic approach
Dirac massless fermions
+
 Renormalization Group
Electron and phonon
renormalization
 of the EPC vertex
Interplay of Coulomb and electron-phonon interactions in graphene
D. M. Basko and I. L. Aleiner
Phys. Rev. B 77, 041409(R) (2008)