Linear response Theory
Claudio Attaccalite
http://attaccalite.com
[Speaker Notes: In an experiment like optical absorption we explore the probability of creating neutral excitations – no particle added or removed from the system -> optical gap]

---
Absorption Spectroscopy I
Many Body Effects!!!
-
+
-
h%nu

---
Absorption Spectroscopy II
Light absorption and transmission is related to the real and imaginary part of the dielectric constant

---
Energy electron-loss Spectroscopy

---
From Maxwell equations
to response functions
Materials equations:
D(r,t) = %epsilon_0 E(r,t) + P(r,t)
From Gauss's law:
nabla cdot E(r,t) = 4 %pi %rho_{tot} (r,t) newline nabla cdot D(r,t) = 4 %pi %rho_{ext} (r,t)
Electric Field
Polarization
Electric Displacement

---
From Maxwell equations
to response functions
Materials equations:
D(r,t) = %epsilon_0 E(r,t) + P(r,t)
From Gauss's law:
nabla cdot E(r,t) = 4 %pi %rho_{tot} (r,t) newline nabla cdot D(r,t) = 4 %pi %rho_{ext} (r,t)
Electric Field
Polarization
Electric Displacement
In general:
P(r,t) = int %chi (t-t',r,r') E(t'r') dt'dr' + int dt^1 dt^2 %chi^2(...) E(t^1) E(t^2) + O(E^3)

---
From Maxwell equations
to response functions
Materials equations:
D(r,t) = %epsilon_0 E(r,t) + P(r,t)
From Gauss's law:
nabla cdot E(r,t) = 4 %pi %rho_{tot} (r,t) newline nabla cdot D(r,t) = 4 %pi %rho_{ext} (r,t)
Electric Field
Polarization
Electric Displacement
In general:
P(r,t) = int %chi (t-t',r,r') E(t'r') dt'dr' + int dt^1 dt^2 %chi^2(...) E(t^1) E(t^2) + O(E^3)
For a small perturbation we consider
only the first term: the linear response
P(r,t) = int %chi (t-t',r,r') E(t'r') dt'dr'
P( %omega ) = %epsilon_0 %chi ( %omega) E( %omega) = %epsilon_0 ( %epsilon (%omega) -1 ) E(%omega)
In Fourier space:
D( %omega ) = %epsilon_0 %epsilon (%omega) E(%omega)

---
Response Functions
Moving from Maxwell equation
to linear response theory we define
%epsilon (%omega) = { D(%omega) } over { %epsilon_0 E(%omega) } = { %delta V_{ext} (%omega) } over { %delta V_{tot} (%omega) }
%epsilon^{-1} (%omega) = { %delta V_{tot} (%omega) } over { %delta V_{ext} (%omega) }
where
V_{tot}(vec r, t)= V_{ext}(vec r, t) + V_{ind} ( vec r, t')
The induced charge density results in a total potential via the Poisson equation:
V_{tot}(vec r t)= V_{ext}(vec r t) + int dt' int d {vec r}^{'} v(vec r-{vec r}^{'}) %rho_{ind}({vec r}^{'} t^{'})
%epsilon^{-1} (%omega) = 1 + v { %delta %rho_{ind} } over { %delta V_{ext} } newline %epsilon (%omega) = 1 - v { %delta %rho_{ind} } over { %delta V_{tot} }
Our goal is to calculate
the derivatives of the induced
density respect to the external potential
%rho_{ind} V_{ind} V_{tot}

---
How to calculated the dielectric constant
%chi(vec r t,{vec r}^{'} t^{'})= { %delta %rho^{ind}(r,t) } over { %delta V _{tot} (r',t') }
We want to calculate:
We expand X, r and V in an independent particle basis set
%chi(bold r t,{bold r}^{'} t^{'})= sum from {i,j,l,m bold k} %chi_{ i,j, l,m} %phi_{i}(r) %phi^{ {} *{} } _{j}(r) %phi_{l} (r')%phi^{ {} * {} }_{m} (r')
%rho(bold r,t )= sum from {n_1, n_2} %varphi_{n_1} (bold r) %varphi^{ {} * {} }_{n_2} (bold r) %rho_{ n_1, n_2 } ( t)
%chi_{ i,j, l,m} = { partial {hat %rho}_{i,j} } over { partial V_{l,m}}
Response function in a single-particle basis set
Density Matrix
i { partial {hat %rho}(t) } over { partial t} = [ H, {hat %rho} ]
The Von Neumann equation
(see Wiki http://en.wikipedia.org/wiki/Density_matrix)

---
Choosing a description for the electronic system
Single-particle Hamiltonian:
Independent particles:
H⁰ (%rho) = T_e + V_{ e -N } + V_H [ color blue %rho^0 ] + V_{ xc} [ color blue %rho^0 ]
Time-dependent Hartree:
H_{Hartree} (%rho) = T_e + V_{ e -N } + V_H [ color red %rho ] + V_{ xc} [ color blue %rho^0 ]
Time-dependent DFT:
H_{KS} (%rho) = T_e + V_{ e -N } + V_H [ color red %rho ] + V_{ xc} [ color red %rho ]
[Speaker Notes: \hat{H}^0 = \hat{T}_e+V_{e-N}+\hat{V}^H [\rho^0] + \hat{\Sigma}^{x} [\rho^0]]

---
Choosing a description for the electronic system
Single-particle Hamiltonian (IP)
H⁰ (%rho) = T_e + V_{ e -N } + V_H [ color blue %rho^0 ] + V_{ xc} [ color blue %rho^0 ]
Single-particle energies
Bloch function

---
Choosing a description for the electronic system
Single-particle Hamiltonian (IP)
H^0 (%rho) = T_e + V_{ e -N } + V_H [ color blue %rho^0 ] + V_{ xc} [ color blue %rho^0 ]
Equilibrium particle density
State occupations
[at zero T and for semiconductors either 0 or 1
otherwise Fermi distribution f(En)]
[Speaker Notes: \rho^0 is diagonal in the Bloch states and time-independent]

---
Time-dependent Hamiltonian and density matrix
Full Hamiltonian
hat H (t) = H^0 + U (t)
hat H (t) = T_e + V_{ e -N } + V_H [ color blue %rho^0 ] + V_{ xc} [ color blue %rho^0 ] + U (t)
Total field
[Speaker Notes: \hat{H}(t) = \hat{H}^0+\hat{U}(t)+\Delta\hat{V}^H [\rho(t)] + \Delta\hat{\Sigma}^{x} [\rho(t)]]

---
Equation of motion
For the density matrix (for more info attend Real Time lecture):
[Speaker Notes: \mathrm{i}\frac{\partial}{\partial t}\rho_{n_1 n_2} (t) = \left[ \hat{H}(t), \hat{\rho}(t)\right]_{n_1 n_2}]

---
Equation of motion
For the density matrix (for more info attend Real Time lecture):
For the response function (taking the functional derivative of the above):
The solution of this equation will yield the linear response
[Speaker Notes: \mathrm{i}\frac{\partial}{\partial t}\chi_{\substack{n_1 n_2 \\ n_3 n_4}} (t,t^\prime) = \frac{\delta}{\delta U_{n_3 n_4}(t^\prime)} \left[ \hat{H}(t), \hat{\rho}(t)\right]_{n_1 n_2}]

---
Solving the equation of motion
A
B
[Speaker Notes: \mathrm{i}\frac{\partial}{\partial t}\chi_{\substack{n_1 n_2 \\ n_3 n_4}} (t,t^\prime) &= \frac{\delta}{\delta U_{n_3 n_4}(t^\prime)} \left[ \hat{H}^0(t), \hat{\rho}(t)\right]_{n_1 n_2} \\ &+ \frac{\delta}{\delta U_{n_3 n_4}(t^\prime)} \left[ \hat{U}(t), \hat{\rho}(t)\right]_{n_1 n_2} \\ &+ \frac{\delta}{\delta U_{n_3 n_4}(t^\prime)} \left[ -\sum_{\substack{m_1 m_2 \\ m_3 m_4}}\int \mathrm{d} \overline{\overline{t}}       \left( \hat{W}-2\hat{V} \right)  \chi^R_{\substack{m_3 m_4 \\ m_1 m_2}}\delta U_{m_1 m_2} (\overline{\overline{t}}), \hat{\rho}(t)\right]_{n_1 n_2}]

---
Solving the equation of motion
Computing the commutators…
A

---
Solving the equation of motion
Computing the commutators…
A
We stay at 1st order in U
B
[Speaker Notes: \left[\hat{U}(t),\hat{\rho}(t)\right]_{n_1 n_2}&=\left[\hat{U}(t),\hat{\rho}^0\right]_{n_1 n_2} \\ &=(f_{n_2}-f_{n_1})U_{n_1 n_2}(t)]

---
Solving the equation of motion
Computing the derivative…
i {partial } over {partial t} %chi_{ binom {n_1, n_2} {n_3, n_4} } ( t, t') = ( E_{n_1} - E_{n_2} ) %chi_{ binom {n_1, n_2} {n_3, n_4} } ( t,t') + ( f_{n2}-f_{n1} ) %delta_{n_1,n_3} %delta_{n_2,n_4} %delta( t-t')
And Fourier transform respect to t-t', we get:
%chi^0_{n_1, n_2, n_3, n_4} ( %omega) = { f_{n_2} - f_{n_1} } over { hbar %omega - ( E_{n_2} - E_{n_1} ) + i %eta} %delta_{n_1,n_3} %delta_{n_2,n_4}
Occupation factor selects transitions from valence to conduction
The poles of the X0
are centered at energy differences
[Speaker Notes: K_{\substack{n_1 n_2 \\ m_3 m_4}} = W_{\substack{n_1 m_4 \\ m_3 n_2}} - 2\left[V^{q_v=0} \right]_{\substack{n_1 n_2 \\ m_3 m_4}} \mathrm{i}\frac{\partial}{\partial t}\chi_{\substack{n_1 n_2 \\ n_3 n_4}} (t-t^\prime) &= (E_{n_1}-E_{n_2})\chi_{\substack{n_1 n_2 \\ n_3 n_4}}(t-t^\prime) \\ &+\mathrm{i}(f_{n_2}-f_{n_1})\left[ -\mathrm{i}\delta_{n_1 n_3}\delta_{n_2 n_4} + \sum_{m_3 m_4} K_{\substack{n_1 n_2 \\ m_3 m_4}} \chi_{\substack{m_3 m_4 \\ n_3 n_4}}(t-t^\prime)\right]]

---
From c(w) to e(w)
Once we have c(w) we just use the formulas
of the first slides to reconstruct epsilon
%varepsilon(%omega) = 1 - 4 %pi %chi^0(%omega, bold q) = 1 - 4 %pi sum_{v,c} { { langle %phi_v abs r %phi_c rangle langle %phi_c abs r %phi_v rangle } over { hbar %omega - (E_{c} - E_{v}) + i %eta}}
[Speaker Notes: K_{\substack{n_1 n_2 \\ m_3 m_4}} = W_{\substack{n_1 m_4 \\ m_3 n_2}} - 2\left[V^{q_v=0} \right]_{\substack{n_1 n_2 \\ m_3 m_4}} \mathrm{i}\frac{\partial}{\partial t}\chi_{\substack{n_1 n_2 \\ n_3 n_4}} (t-t^\prime) &= (E_{n_1}-E_{n_2})\chi_{\substack{n_1 n_2 \\ n_3 n_4}}(t-t^\prime) \\ &+\mathrm{i}(f_{n_2}-f_{n_1})\left[ -\mathrm{i}\delta_{n_1 n_3}\delta_{n_2 n_4} + \sum_{m_3 m_4} K_{\substack{n_1 n_2 \\ m_3 m_4}} \chi_{\substack{m_3 m_4 \\ n_3 n_4}}(t-t^\prime)\right]]

---
Local field effects (RPA)
H_{Hartree} (%rho) = T_e + V_{ e -N } + V_H [ color red %rho ] + V_{ xc} [ color blue %rho^0 ]
This is a matrix equation
Following similar derivation we get an equation for c:
%chi(%omega,bold q)_{bold G_1, bold G_2} = %chi^0_{bold G_1, bold G_2} (%omega,bold q) + %chi^0_{bold G_1, bold G_3} (%omega,bold q) v_{bold G_3} %chi (%omega,bold q)_{bold G_3, bold G_2}
%chi^0(%omega, bold q)_{bold G_1, bold G_2} = sum_{v,c} { { langle %phi_v abs e^{-i(bold q + bold G_1) r} %phi_c rangle langle %phi_c abs e^{i(bold q + bold G_2) r' } %phi_c rangle } over { hbar %omega - (E_{c} - E_{v} ) + i %eta}}
where
And the epsilon has always the form:
%varepsilon(%omega,bold q)= 1 - 4 %pi %chi (%omega,bold q)_{0,0}
[Speaker Notes: K_{\substack{n_1 n_2 \\ m_3 m_4}} = W_{\substack{n_1 m_4 \\ m_3 n_2}} - 2\left[V^{q_v=0} \right]_{\substack{n_1 n_2 \\ m_3 m_4}} \mathrm{i}\frac{\partial}{\partial t}\chi_{\substack{n_1 n_2 \\ n_3 n_4}} (t-t^\prime) &= (E_{n_1}-E_{n_2})\chi_{\substack{n_1 n_2 \\ n_3 n_4}}(t-t^\prime) \\ &+\mathrm{i}(f_{n_2}-f_{n_1})\left[ -\mathrm{i}\delta_{n_1 n_3}\delta_{n_2 n_4} + \sum_{m_3 m_4} K_{\substack{n_1 n_2 \\ m_3 m_4}} \chi_{\substack{m_3 m_4 \\ n_3 n_4}}(t-t^\prime)\right]]

---
Beyond IPA e(w) is a matrix!
Notice that beyond independent particle approximation the e(w) is a matrix therefore:
%varepsilon (%omega,bold q) = {1} over { [ %varepsilon (%omega,bold q) ]^{-1}_{ bold G=0, bold {G'}=0} }
%varepsilon (%omega,bold q) <> { 1 } over { %varepsilon^{ -1} (%omega,bold q)}
... but:
This makes the difference between the EELS and Absorption spectra
[Speaker Notes: K_{\substack{n_1 n_2 \\ m_3 m_4}} = W_{\substack{n_1 m_4 \\ m_3 n_2}} - 2\left[V^{q_v=0} \right]_{\substack{n_1 n_2 \\ m_3 m_4}} \mathrm{i}\frac{\partial}{\partial t}\chi_{\substack{n_1 n_2 \\ n_3 n_4}} (t-t^\prime) &= (E_{n_1}-E_{n_2})\chi_{\substack{n_1 n_2 \\ n_3 n_4}}(t-t^\prime) \\ &+\mathrm{i}(f_{n_2}-f_{n_1})\left[ -\mathrm{i}\delta_{n_1 n_3}\delta_{n_2 n_4} + \sum_{m_3 m_4} K_{\substack{n_1 n_2 \\ m_3 m_4}} \chi_{\substack{m_3 m_4 \\ n_3 n_4}}(t-t^\prime)\right]]

---
Take-home message
Linear response is the first order response function to an external field
The choice of the Hamiltonian sets the approximation level in the response function
The dielectric function can calculated summing on all valence conduction transitions
Independent particle approximation is not enough to reproduce experiments
[Speaker Notes: H^{2p}_{\mathcal{K}\mathcal{K}^\prime} = \Delta E_{\mathcal{K}}\delta_{ \mathcal{K} \mathcal{K}^\prime} + \mathrm{i} \mathcal{F}_{\mathcal{K}} K_{\mathcal{K}\mathcal{K}^\prime}]

---
References:
[Speaker Notes: H^{2p}_{\mathcal{K}\mathcal{K}^\prime} = \Delta E_{\mathcal{K}}\delta_{ \mathcal{K} \mathcal{K}^\prime} + \mathrm{i} \mathcal{F}_{\mathcal{K}} K_{\mathcal{K}\mathcal{K}^\prime}]