Optical properties
of hexagonal boron nitride
(new experiments and theory)
Claudio Attaccalite
L. Artús, A. Segura.
M. Feneberg, J. H. Edgar, J. Li, R. Goldhahn, T. Taniguchi, K. Watanabe, R. Cuscód

---
hBN-encapsulated 2D materials

---
hBN is one of the
preferred materials by theoreticians

---
hBN is one of the
preferred materials by theoreticians
Tight-binding
F. Paleari et al 2018 2D Mater. 5 045017
L. Sponza et al. Phys. Rev. B 98, 125206(2018)

---
hBN is one of the
preferred materials by theoreticians
Exciton-phonon coupling
Tight-binding
F. Paleari et al 2018 2D Mater. 5 045017
L. Sponza et al. Phys. Rev. B 98, 125206(2018)
F. Paleari et al PRL. 122, 187401 (2019)
E. Cannuccia et al. PRB 99, 081109(R)(2019)

---
hBN is one of the
preferred materials by theoreticians
2D exciton dispersion
Exciton-phonon coupling
Tight-binding
P. Cudazzo PRL 116, 066803 (2016)
F. Paleari et al 2018 2D Mater. 5 045017
L. Sponza et al. Phys. Rev. B 98, 125206(2018)
F. Paleari et al PRL. 122, 187401 (2019)
E. Cannuccia et al. PRB 99, 081109(R)(2019)

---
hBN is one of the
preferred materials by theoreticians
2D exciton dispersion
Exciton-phonon coupling
Tight-binding
P. Cudazzo PRL 116, 066803 (2016)
F. Paleari et al 2018 2D Mater. 5 045017
L. Sponza et al. Phys. Rev. B 98, 125206(2018)
F. Paleari et al PRL. 122, 187401 (2019)
E. Cannuccia et al. PRB 99, 081109(R)(2019)
Exictons in
non-linear response
C. Attaccalite et al. PRB 98 165126 (2018)
T. G. Pedersen, PRB 92, 235432 (2015)

---
hBN is one of the
preferred materials by theoreticians
2D exciton dispersion
Exciton-phonon coupling
Tight-binding
P. Cudazzo PRL 116, 066803 (2016)
F. Paleari et al 2018 2D Mater. 5 045017
L. Sponza et al. Phys. Rev. B 98, 125206(2018)
F. Paleari et al PRL. 122, 187401 (2019)
E. Cannuccia et al. PRB 99, 081109(R)(2019)
Exictons in
non-linear response
2D phonon dispersion
T. Sohier et al. NanoLetters 17, 3758 (2017)
C. Attaccalite et al. PRB 98 165126 (2018)
T. G. Pedersen, PRB 92, 235432 (2015)

---
hBN is one of the
preferred materials by theoreticians
2D exciton dispersion
Exciton-phonon coupling
Tight-binding
F. Paleari et al 2018 2D Mater. 5 045017
L. Sponza et al. Phys. Rev. B 98, 125206(2018)
F. Paleari et al PRL. 122, 187401 (2019)
E. Cannuccia et al. PRB 99, 081109(R)(2019)
P. Cudazzo PRL 116, 066803 (2016)
J. Koskelo et al. PRB 95, 035125 (2017)
Exictons in
non-linear response
Benchmark
for total energy
2D phonon dispersion
T. Sohier et al. NanoLetters 17, 3758 (2017)
C. Attaccalite et al. PRB 98 165126 (2018)
T. G. Pedersen, PRB 92, 235432 (2015)
T.Gruber et al. PRX 8, 021043 (2018)

---
All theory compares with epsilon reconstructed from inelastic electronic scattering
C. Tarrio and S. E. Schnatterly PRB 40, 7852 (1989)

---
Ellipsometry Study of Hexagonal Boron Nitride using Synchrotron Radiation

---
Ellipsometry Study of Hexagonal Boron Nitride using Synchrotron Radiation

---
Theory vs experiments 1/2
….perfect agreement?...
	First Exciton
Exp.	6.12 eV
GoWo + BSE	5.76 eV
evGW + BSE	6.03 eV
QSGW + BSE PRM 2, 034603 (2018)	6.11 eV

---
Theory vs experiments 1/2
….perfect agreement?...
Electron-phonon	DGap
PRB 99, 165201 (2019)	0.273 eV
PRB 101, 205115 (2020)	0.35 eV (0.4 at 300K)
PRB 102, 045117 (2020)	0.2 eV
	First Exciton
Exp.	6.12 eV
GoWo + BSE	5.76 eV
evGW + BSE	6.03 eV
QSGW + BSE PRM 2, 034603 (2018)	6.11 eV
Reduction exciton binding energy PRL 101,106405 (2008)	30% * 0.8eV = 0.26 eV
and more: vertex correction, phonon screening

---
Theory vs experiments 2/2
High energy excitations

---
Theory vs experiments 2/2
High energy excitations
Take home message:
hBN is transparent in the UVC
the radiation that kills Coronavirus

---
hBN at finite pressure
Sapphire anvils
These are not trivial experiments, as conventional diamond anvil cells cannot be used to optically access the bandgap spectral range of h-BN. Instead, one has to use
sapphire anvils, which are rather brittle and prone to crack easily under pressure.

---
Reflectance spectra of h-BN
under pressure

---
h-BN under pressure: atomic structure

---
hBN under pressure: the band structure
A Unified Understanding of the Thickness-Dependent Bandgap Transition in Hexagonal Two-Dimensional Semiconductors
Kang, J.; Zhang, L.; Wei, S.-H. , J. Phys. Chem. Lett. 2016, 7, 597−602 (2016)

---
hBN under pressure: excitons
Excitons decomposition
Gaps and excitons
under pressure

---
hBN under pressure: excitons
 Exciton binding energies
as a function of pressure
Gaps and excitons
under pressure

---
Experiments vs theory
Direct and indirect excitonic transitions determined from the reflectance spectra compared with the ab-initio theoretical calculations (solid lines).

---
Conclusions
This is the first ellipsometric study performed with synchrotron radiation in 2D/layered compounds. This allowed us to determine the dielectric constant of h-BN over an extended energy range up to 25 eV
We have investigated the pressure-induced shifts of direct and indirect excitonic transitions of the indirect-bandgap bulk h-BN layered crystal.
References
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC
Luis Artús, M. Feneberg, C. Attaccalite, J. H. Edgar, J. Li, R. Goldhahn, Ramon Cuscó, https://doi.org/10.1002/adpr.202000101
Tuning the Direct and Indirect Excitonic Transitions of h‐BN by Hydrostatic Pressure
A. Segura, R. Cuscó, C. Attaccalite, T. Taniguchi, K. Watanabe, and L. Artús, in press

---
Reflectivity and reflectance
Calculated reflectivity spectrum associated with the direct excitonic transitions (dashed line), compared with the experimental reflectance measurement (red dots). The blue and green sigmoidal dotted lines account for, respectively, the drop of reflectance due to the absorption at the direct and indirect excitonic energies suppressing the reflection at the bottom interface. The solid line is the resulting calculated reflectance after taking into account the self-absorption effect.