Theory of phonon-assisted luminescence: application to h-BN
Claudio Attaccalite

---
Opto-electronic devices

---
Light emission

---
The problem of indirect semiconductors
Indirect band gap semiconductors are not good for photonics/optoelectronics

---
Silicon Laser : solutions
Defects
Nanostructures
and more…. hybrid lasers etc...

---
Silicon Laser in the news

---
The other colors and the UV

---
Hexagonal Boron Nitride
h-BN is a layered
crystal homo-structural to graphite.
As graphite, h-BN can be easily exfoliated, and for this reason it finds applications as lubricant .

---
Hexagonal Boron Nitride
h-BN has a large band gap and it’s transparent
h-BN emits light in the ultraviolet

---
Breaking news
on h-BN !!!
Direct-bandgap properties and evidence for ultraviolet lasing of h-BN single crystal
K. Watanabe et al. Nature Materials 3, 404 (2004)*

---
Breaking news
on h-BN !!!
Direct-bandgap properties and evidence for ultraviolet lasing of h-BN single crystal
K. Watanabe et al. Nature Materials 3, 404 (2004)*
Hexagonal boron nitride is an indirect band-gap semiconductor
G. Cassabois et al., Nature Photonics, 10, 262 (2016)*
*) results from Luminescence measurements

---
Internal quantum yield
ZnO
Bright Luminescence from Indirect and Strongly Bound Excitons in h-BN
L. Schué, L. Sponza et al.,
Phys. Rev. Lett. 122, 067401(2019)
50%

---
Internal quantum yield
Diamond
ZnO
Bright Luminescence from Indirect and Strongly Bound Excitons in h-BN
L. Schué, L. Sponza et al.,
Phys. Rev. Lett. 122, 067401(2019)
50%
0.1%

---
Internal quantum yield
Diamond
hBN
ZnO
Bright Luminescence from Indirect and Strongly Bound Excitons in h-BN
L. Schué, L. Sponza et al.,
Phys. Rev. Lett. 122, 067401(2019)
45%
0.1%
50%

---
h-BN band structure and ARPES
Direct observation of the band structure in bulk hexagonal boron nitride
H. Henck, et al.
PRB 95, 085410(2017)

---
h-BN optical properties 1/2
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC
L. Artús, M. Feneberg, C. Attaccalite, J. H. Edgar, J. Li, R. Goldhahn, R. Cuscó,
Advanced Photonics Research 2 (5), 2000101 (2021)

---
h-BN optical properties 1/2
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC
L. Artús, M. Feneberg, C. Attaccalite, J. H. Edgar, J. Li, R. Goldhahn, R. Cuscó,
Advanced Photonics Research 2 (5), 2000101 (2021)

---
h-BN optical properties 2/2
Take home message:
hBN is transparent in the UVC
the radiation that kills Coronavirus

---
Electron loss spectroscopy on h-BN

---
May we probe indirect nature of h-BN with EELS?
Direct Observation of the Lowest Indirect Exciton State in the Bulk
of Hexagonal Boron Nitride
R. Schuster C. Habenicht, M. Ahmad, M. Knupfer, B. Büchner,
PRB 97, 041201 (2018)

---
Origin of the EELS peaks
Loss function
 Peaks of L(q, ω) can be put in relation to inter-band excitations (∝ Im[ε(q, ω)])
and plasmon resonances (|ε| ≈ 0)
Direct Observation of the Lowest Indirect Exciton State in the Bulk of Hexagonal Boron Nitride
R. Schuster C. Habenicht, M. Ahmad, M. Knupfer, B. Büchner, PRB 97, 041201 (2018)
Exciton interference in hexagonal boron nitride
L. Sponza, H. Amara, C. Attaccalite, F. Ducastelle, A. Loiseau
PRB 97 (7), 075121(2017)

---
What about luminescence?

---
Phonon-assisted
absorption and emission
Average on phonon modes
Derive BSE in presence of EPC
(first order, cumulant)
%XI = {partial %SIGMA} over { partial G }
Perturbation Theory
in the excitonic space
Polaron transformation

---
Average on phonons
Average
on phonon modes
+non-perturbative
+an-harmonic effects
-no dynamical effects
-supercells
Stochastic Approach to Phonon-Assisted Optical Absorption
M. Zacharias, C. E. Patrick, and F. Giustino
Phys. Rev. Lett. 115, 177401(2015)
Electron–phonon coupling from finite differences
B. Monserrat
J. of Phys.: Cond. Matt. 30, 083001(2018)

---
Bethe-Salpeter Eq.
with Electron-phonon
First order
self-energy or cumulant etc..
+dynamical effects
+no-supercells
-complicated eqs.
-dynamics BSE
First-principles description of the exciton-phonon interaction: A cumulant approach
Pierluigi Cudazzo
Phys. Rev. B 102, 045136(2020)
Theory of exciton-phonon coupling
 G. Antonius and S. G. Louie,
arXiv:1705.04245

---
Polaron transformation
+stardard BSE
+non-perturbative
-difficult improv.?
 Phonon sidebands in semiconductor luminescence T. Feldtmann, M. Kira, and S. W. Koch
Phys. Stat. Solidi B 246, 332(2009)
Phonon-assisted luminescence ..
A. Chernikov, et al.
Phys. Rev. B 85, 035201(2012)

---
Perturbation theory
in the excitonic space
+simple eqs.
-miss no-exc terms.
-high orders more difficult
Phonon and Electronic Nonradiative Decay Mechanisms of Excitons in Carbon Nanotubes
V.i Perebeinos and P. Avouris
Phys. Rev. Lett. 101, 057401 (2008)
Effect of Exciton-Phonon Coupling in the Calculated Optical Absorption of Carbon Nanotubes
V. Perebeinois, J. Tersoff, P. Avoris
PRL 94, 027402(2005)

---
Luminescence Theory
Non-equilibrium Bethe-Salpeter equation
In the limit of low excited carriers
Emission
Absorption
%varepsilon( %omega ) = sum_{ %lambda } %PI_{%lambda} %delta(%omega - E_{%lambda})
I ( %omega ) prop sum_{ %lambda } %PI_{%lambda} f^{{}<{}}_{%lambda } %delta(%omega - E_{%lambda})
f^{{}<{}}_{%lambda } = sum_{K} langle %lambda divides K rangle f^{{ }<{} }_K langle K divides %lambda rangle
f^{{ }<{} }_K = f_c ( 1-f_v )
NON-EQUILIBRIUM GREEN’S FUNCTION
Theory of photoluminescence in semiconductors
K. Hannewald, S. Glutsch, and F. Bechstedt
PRB 62, 4519 (2000).
DENSITY MATRIX
Semiconductor Quantum Optics
M. Kira and S. W. Koch
Cambridge Univ. Press. (2012).

---
Time-dependent perturbation
theory in the excitonic space
perturbative correction of the BSE due to the electron-phonon coupling
+
electron-phonon matrix elements calculated
by finite difference
We constructed a non-diagonal supercell that maps K and M points at G
Infrared absorption spectrum of germanium
LH. Hall, J. Bardeen, FJ. Blatt
Phys. Rev., 95, 559 (1954)
Electron–phonon coupling from finite differences
B. Monserrat
J. of Phys.: Cond. Matt. 30, 083001(2018)

---
Which phonons are involved
in luminescence?
T

---
Luminescence in h-BN
Theory*
Theory of phonon-assisted luminescence in solids: application to hexagonal boron nitride
E Cannuccia,et al.
Rev. B 99, 081109(R) (2019)
Experiment
Hexagonal boron nitride is an indirect band-gap semiconductor
G. Cassabois et al.,
Nature Photonics, 10, 262 (2016)
 similar results obtained also by:
F. Paleari et al. PRL 122, 187401 (2019) and HY. Chen et al. PRL 125, 107401 (2020) and additional modeling in PRL 127, 137401 (2021)

---
Conclusions
The indirect nature of hBN can be probed by EELS
We obtained the first measurement of optical absorption of a layered material by ellipsometry using synchrotron radiation
We extended luminescence theory to include phonon scattering and reproduce the luminescence spectra
Codes
References
Exciton interference in hexagonal boron nitride
L. Sponza, H. Amara, C. Attaccalite, F. Ducastelle, A. Loiseau
Phys. Rev. B 97, 075121 (2017)
Theory of phonon-assisted luminescence in solids: application to hexagonal boron nitride
E. Cannuccia, B. Monserrat and C. Attaccalite
Rev. B 99, 081109(R) (2019)
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC
L. Artús, M. Feneberg, C. Attaccalite, J. H. Edgar, J. Li, R. Goldhahn, R. Cuscó,
Advanced Photonics Research 2 (5), 2000101 (2021)

---
Acknowledgments
Bartomeu Monserrat
Elena Cannuccia
Elena Cannuccia
Lorenzo Sponza
Hakim Amara
François Ducastelle
L. Wirtz, M. Gruning, F. Paleari, S. Latil

---
Luminescence intensity
from bulk to monolayer
This ratio in MoS2 is about 104
Dimensionality effects on the luminescence properties of hBN
L. Schué et al., Nanoscale 8, 6986 (2016).
Excitons in few-layer hexagonal boron nitride: Davydov splitting and surface localization
F. Paleari, et al. 2D Materials 5, 045017 (2018)

---
What next?
 Temperature dependence of luminescence
 Higher-order
phonon sidebands
Overtones of interlayer shear modes in the phonon-assisted emission spectrum of hexagonal boron nitride.
T. Q. P. Vuong et al,
PRB, 95(4), 045207 (2017)
Bright Luminescence from Indirect and Strongly Bound Excitons in h-BN
L. Schué, L. Sponza et al.,
Phys. Rev. Lett. 122, 067401(2019)

---
Time-dependent perturbation
theory in the excitonic space 1/3
We start with the electron-phonon Hamiltonian:
We start with the electron-phonon Hamiltonian:
electron-phonon coupling in the two-particle basis
rotation in the excitonic basis
 First order correction to the excitonic wave-functions:

---
Time-dependent perturbation
theory in the excitonic space 2/3
Use the new wave-function to calculate emission and absorption
Phonon Absorption
Phonon Emission
perturbative correction to the dipoles can be mapped in a derivative
respect to the phonon mode
One-shot calculation of temperature-dependent optical spectra ..
M. Zacharias and F. Giustino
 Physical Review B 94, 075125 (2016).

---
Theory vs experiments
Angular resolved electron energy loss spectroscopy in hexagonal boron nitride
F. Fossard et al. Phys. Rev. B 96 115304 (2017)

---
Theory: how to calculate e(w)
Excitons in boron nitride single layer
T. Galvani et al., Phys. Rev. B 94, 125303 (2016)
G. Strinati, Nuovo Cimento 11, 1 (1988)

---
EELS - theory and experiments
Exciton interference in hexagonal boron nitride
L. Sponza, et al.
PRB 97(7), 075121(2017)