Quantum Espresso code
http://www.quantum-espresso.org/

---
Quantum Espresso code
Different executables for different tasks in QEDIR/bin
Documentation in QEDIR/Doc/INPUT_XX.txt
Code organization
pw.x	main code
pp.x	data analysis
ph.x	phonons/electron-phonon coupling
dos.x	density of states
bands.x plot band structure
pwcond.x transmitance
cp.x molecular dynamics
more tools avilable:
x-ray spectra, optics ,EELS, superconductivity,
magnetic resonance (NMR) etc..

---
Typical input file
 &control
    prefix='silicon',
    pseudo_dir='./'
    outdir = ‘./',
 /
 &system
    ibrav= 2,
    celldm(1) =10.2,
    nat= 2,
    ntyp= 1,
    ecutwfc = 12.0,
 /
 &electrons
 /
ATOMIC_SPECIES
 Si 28.086 Si.dojo.UPF
ATOMIC_POSITIONS {crystal}
 Si 0.00 0.00 0.00
 Si 0.25 0.25 0.25
K_POINTS automatic
2 2 2 0 0 0

---
Bravais Lattices: ibrav flag
https://en.wikipedia.org/wiki/Bravais_lattice
ibrav =1,3,2
ibrav =6, 7
ibrav =8, 9, 10, 11
ibrav =4, 5, -5
ibrav =12, -12, 13
ibrav =14

---
Typical input file
 &control
    prefix='silicon',
    pseudo_dir='./'
    outdir = ‘./',
 /
 &system
    ibrav= 2,
    celldm(1) =10.2,
    nat= 2,
    ntyp= 1,
    ecutwfc = 12.0,
 /
 &electrons
 /
ATOMIC_SPECIES
 Si 28.086 Si.dojo.UPF
ATOMIC_POSITIONS {crystal}
 Si 0.00 0.00 0.00
 Si 0.25 0.25 0.25
K_POINTS automatic
2 2 2 0 0 0

---
Typical input file
 &control
    prefix='silicon',
    pseudo_dir='./'
    outdir = ‘./',
 /
 &system
    ibrav= 2,
    celldm(1) =10.2,
    nat= 2,
    ntyp= 1,
    ecutwfc = 12.0,
 /
 &electrons
 /
ATOMIC_SPECIES
 Si 28.086 Si.dojo.UPF
ATOMIC_POSITIONS {crystal}
 Si 0.00 0.00 0.00
 Si 0.25 0.25 0.25
K_POINTS automatic
2 2 2 0 0 0

---
Pseudo-potentials of this tutorials
http://www.pseudo-dojo.org/
(QE format is called UPF)

---
Typical input file
 &control
    prefix='silicon',
    pseudo_dir='./'
    outdir = ‘./',
 /
 &system
    ibrav= 2,
    celldm(1) =10.2,
    nat= 2,
    ntyp= 1,
    ecutwfc = 12.0,
 /
 &electrons
 /
ATOMIC_SPECIES
 Si 28.086 Si.dojo.UPF
ATOMIC_POSITIONS {crystal}
 Si 0.00 0.00 0.00
 Si 0.25 0.25 0.25
K_POINTS automatic
2 2 2 0 0 0

---
First calculation:
Self-consistent calculation for Silicon
in the diamond structure
Espace de Travail: tutorials/Si_bulk/
or download from http://attaccalite.com/QE_tutorial/
Unpack files: tar zxvf Si_bulk.tgz
Look the input file:
cd Si_bulk/
gedit/xed/nano/vi/emacs Si.scf.in
Run calculations!!
pw.x -inp Si.scf.in > output_scf

---
Look the output file: check electrons, convergence, etc...

---
 &control
    prefix='silicon',
    pseudo_dir='./'
    outdir = ‘./',
 /
 &system
    ibrav= 2,
    celldm(1) =10.2,
    nat= 2,
    ntyp= 1,
    ecutwfc = 12.0,
 /
 &electrons
 /
ATOMIC_SPECIES
 Si 28.086 Si.dojo.UPF
ATOMIC_POSITIONS {crystal}
 Si 0.00 0.00 0.00
 Si 0.25 0.25 0.25
K_POINTS automatic
2 2 2 0 0 0
First calculation:
Converge the total energy with respect
to G-vectors and K-points
You can use ‘gnuplot’ or ‘xmgrace’

---
Using Xcrysden to verify input/output

---
Using Xcrysden to verify input/output

---
What can we do with the total energy?
Structure optimization, phonons, compressibility, phase transitions, binding energy, etc...

---
Second calculation:
Optimal lattice parameter for Silicon

---
Third calculation:
Silicon band structure (Si.nscf.in)
 &control
    calculation=’nscf’,
    prefix='silicon',
    pseudo_dir='./'
    outdir = ‘./',
 /
 &system
    ibrav= 2,
    celldm(1) =10.2,
    nat= 2,
    ntyp= 1,
    ecutwfc = 12.0,
    nbnd=8
 /
 &electrons
 /
ATOMIC_SPECIES
 Si 28.086 Si.vbc.UPF
ATOMIC_POSITIONS {crystal}
 Si 0.00 0.00 0.00
 Si 0.25 0.25 0.25
K_POINTS crystal_b
3
0.5 0.5 0.5 20
0.0 0.0 0.0 20
0 0.5 0.5 10
New calculation type
Number of bands
k-points list using crystal_b
(generate a path in k-space)

---
Bands plot
 &bands
    prefix = 'silicon'
    outdir='./'
    filband = 'bands.dat'
 /
bands.in file
Run bands.x
bands.x < bands.in > output_scf
Plot with gnuplot
gnuplot
gnuplot> plot ‘bands.dat.gnu’ u 1:2 w l

---
4th calculation: data analysis
Charge density
  &inputpp
    prefix = 'silicon'
    outdir='./'
    filplot = 'sicharge'
    plot_num= 0
 /
 &plot
    iflag = 3
    output_format = 5
    fileout = 'si.rho.xsf'
 /
Run pp.x
pp.x < si.pp_rho.in > output_pp
Visualize with Xcrysden
xcrysden --xsf si.rho.xsf

---
Data Visualization with Xcrysden
Tools→ Data grid
Set Isolevel

---
Structure optimization

---
The king of structure optimization
Among the highlights are the discovery of the structure of a superhard phase of boron, gamma-B, transparent phase of sodium, new carbon allotrope, stability of MgSiO3 post-perovskite in the Earth's mantle, prediction and synthesis of "forbidden" compounds (e.g., Na3Cl), discovery of helium chemistry, and creation of borophene - a 2D-monolayer of boron atoms, with great promises for future technologies
see wiki for references.
Artem Oganov
https://en.wikipedia.org/wiki/Artem_R._Oganov

---
Why you will not be as successful
as Artem Organov
Energy landscape too complex
Artem Oganov
https://en.wikipedia.org/wiki/Artem_R._Oganov
Use UPEX!!

---
Structural relaxation
 &control
    calculation= ‘relax’,
    prefix='silicon',
    pseudo_dir='./'
    outdir = ‘./',
 /
 &system
    ibrav= 2,
    celldm(1) =10.2,
    nat= 2,
    ntyp= 1,
    ecutwfc = 12.0,
 /
 &electrons
 /
&ions
  ions_dynamics=’damp’ or ‘BFGS’
/
ATOMIC_SPECIES
 Si 28.086 Si.vbc.UPF
ATOMIC_POSITIONS {crystal}
 Si 0.00 0.00 0.00
 Si 0.25 0.25 0.25
K_POINTS automatic
2 2 2 0 0 0
New calculation type
New namelist
Optimization methods for finding minimum energy paths
J. Chem. Phys. 128, 134106 (2008)

---
Input file for the 3x3 graphene: graphene3x3.in
Input file for the oxygen: oxygen.in
Put the oxygen on the graphene and relax the structure
Calculate the absorption energy
E_abs = E_tot – E_graphene -E_o

---
Data Visualization with Xcrysden
Tools→ Data grid
Set Isolevel