Luminescence of
hexagonal boron nitride monolayer
Claudio Attaccalite
P. Lechifflart, F. Paleari,
D. Sangalli
GDR-REST General Meeting (2023)

---
Use of hBN in condensed matter
Single photon emitters
Encapsulated 2D materials

---
Band structure of hBN

---
Internal quantum yield
Diamond
ZnO
Bright Luminescence from Indirect and Strongly Bound Excitons in h-BN
L. Schué, L. Sponza et al.,
Phys. Rev. Lett. 122, 067401(2019)
0.1%
50%

---
Internal quantum yield
Diamond
hBN
ZnO
Bright Luminescence from Indirect and Strongly Bound Excitons in h-BN
L. Schué, L. Sponza et al.,
Phys. Rev. Lett. 122, 067401(2019)
45%
0.1%
50%

---
Strong bound
excitons in h-BN
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC
Luis Artús, et al. Advanced Photonics Research 2 (5), 2000101 (2021)
No-exciton spectrum

---
Exciton-phonon coupling
The strong exciton confinement enhances the coupling with phonons
Theory of phonon-assisted luminescence in solids:
application to hexagonal boron nitride
E. Cannuccia,et al. Phys. Rev. B 99, 081109(R) (2019)

---
Monolayer hexagonal BN
First Luminescence measurement on epitaxial grown monolayer boron nitride on graphite substrates
Nature Communications volume 10, Article number: 2639 (2019)

---
From bulk to monolayer…..
Direct observation of the band structure in bulk hexagonal boron nitride
H. Henck, et al.
PRB 95, 085410(2017)

---
Luminescence spectra
Nature Communications volume 10, Article number: 2639 (2019)

---
Luminescence spectra … again
Monolayer Boron Nitride: Hyperspectral Imaging in the Deep Ultraviolet
A. Rousseau et al.
Nano Lett. 2021, 21, 23, 10133–10138

---
Luminescence spectra … again
Monolayer Boron Nitride: Hyperspectral Imaging in the Deep Ultraviolet
A. Rousseau et al.
Nano Lett. 2021, 21, 23, 10133–10138
“Scalable Synthesis of Monolayer Hexagonal Boron Nitride on Graphene with Giant Bandgap Renormalization."
Wang et al. Advanced Materials 34.21 (2022).

---
BSE and exciton dispersion
We start from the standard BSE in Tamm-Dancoff approx.

---
BSE and exciton dispersion
We start from the standard BSE in Tamm-Dancoff approx.
Solve the BSE and construct
the corresponding Green’s function

---
BSE and exciton dispersion
We start from the standard BSE in Tamm-Dancoff approx.
Solve the BSE and construct
the corresponding Green’s function
Use L to build the polarization function:

---
Exciton-phonon theory 1/2
Exciton-phonon Hamiltonian in the excitonic basis set

---
Exciton-phonon theory 1/2
Exciton-phonon Hamiltonian in the excitonic basis set
Where the exciton-phonon coupling is defined as

---
Exciton-phonon theory 2/2
Starting from the exciton-phonon Hamiltonian
H(bold Q) = H_{exc} (bold Q) + H_{exc-ph} (bold Q)

---
Exciton-phonon theory 2/2
Starting from the exciton-phonon Hamiltonian
H(bold Q) = H_{exc} (bold Q) + H_{exc-ph} (bold Q)
construct the exciton-phonon self-energy

---
Exciton-phonon theory 2/2
Starting from the exciton-phonon Hamiltonian
H(bold Q) = H_{exc} (bold Q) + H_{exc-ph} (bold Q)
construct the exciton-phonon self-energy
..and solve this Dyson equation at the first order
Renormalization factor:

---
From theory to ab-initio
Boltzman occupation

---
Validation

---
Validation
Phase
mismatch
problem

---
The role of substrate

---
The role of substrate

---
Direct or
indirect excitons

---
LDA+scissor+BSE

---
Theory vs experiments

---
Conclusions
- Monolayer-BN presents only direct light-emission, the phonon assisted one is too weak
- We developed a new approach to study phonon-assisted transitions
Theory of phonon-assisted luminescence in solids: application to hexagonal boron nitride
E. Cannuccia,et al. Phys. Rev. B 99, 081109(R) (2019)
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC, Luis Artús, et al. Advanced Photonics Research 2 (5), 2000101 (2021)
First-principles study of luminescence in hexagonal boron nitride single layer: Exciton-phonon coupling and the role of substrate
P. Lechifflart, et al. Phys. Rev. Mat. 7, 024006 (2023)
Davide Sangalli
Fulvio Paleari
Pierre Lechifflart

---
Conclusions
- Monolayer-BN presents only direct light-emission, the phonon assisted one is too weak
- We developed a new approach to study phonon-assisted transitions
Theory of phonon-assisted luminescence in solids: application to hexagonal boron nitride
E. Cannuccia,et al. Phys. Rev. B 99, 081109(R) (2019)
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC, Luis Artús, et al. Advanced Photonics Research 2 (5), 2000101 (2021)
First-principles study of luminescence in hexagonal boron nitride single layer: Exciton-phonon coupling and the role of substrate
P. Lechifflart, et al. Phys. Rev. Mat. 7, 024006 (2023)
Davide Sangalli
Pierre Lechifflart

---
Solving the phase mismatch problem
Exciton and electron-phonon coupling are calculated using the same single particle Kohn-Sham states.
see M. Zanfrognini et al. https://arxiv.org/abs/2305.17554

---
Conclusions again
- Monolayer-BN presents only direct light-emission, the phonon assisted one is too weak
- We developed a new approach to study phonon-assisted transitions
- Phase mismatch can be solved!! (see arXiv:2305.17554)
Theory of phonon-assisted luminescence in solids: application to hexagonal boron nitride
E. Cannuccia,et al. Phys. Rev. B 99, 081109(R) (2019)
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC, Luis Artús, et al. Advanced Photonics Research 2 (5), 2000101 (2021)
First-principles study of luminescence in hexagonal boron nitride single layer: Exciton-phonon coupling and the role of substrate
P. Lechifflart, et al. Phys. Rev. Mat. 7, 024006 (2023)
Davide Sangalli
Pierre Lechifflart

---
More exciton-phonon interactions
Theory of exciton-phonon coupling
G. Antonius and S. Louie Phys. Rev. B 105, 085111 (2022)

---
The role of substrate on exciton dispersion and luminescence

---
Excitonic occupation and luminescence
Cannuccia E. et al.
PRB 99, 081109® (2019)
Boltzman occupation