Cover
Neutral Electronic Excitations:
a Many-body approach
to the optical absorption spectra
Claudio Attaccalite
http://abineel.grenoble.cnrs.fr/
Second Les Houches school in computational physics:
ab-initio simulations in condensed matter

---
Motivations
Motivations: Absorption Spectroscopy
-
+
-
Many Body Effects!!!
h%nu

---
Motivations(II):Absorption Spectroscopy
Absorption linearly related to the Imaginary part of the MACROSCOPIC dielectric constant (frequency dependent)

---
Outline
Outline
How can we calculate the response of the system? Time Dependent – DFT and Bethe Salpeter Equation
Some applications and recent steps forward
Conclusions
Response of the system to a perturbation →
Linear Response Regime

---
Spectroscopy

---
Theoretical Spectroscopy
Propagation
Correlation
{1} over {r-r'}
Schrödinger eq.
i { partial } over { partial t_1} %PSI = H + V_ext(r,t) %PSI
left [ i { partial } over { partial t_1} + e_i + V_ext right ] G_{ij}(t_1,t_2) = %delta(t_1,t_2) + int %SIGMA G
Green's functions
%SIGMA(t_1,t_2)
i { partial } over { partial t} %rho(t) = [H + V_ext, %rho(t)]
Density Matrix
%rho^2(r,r,r,r), %rho^3.....
i { partial } over { partial t} %varphi = ( V_h + V_xc + V_ext) %varphi + 1/2 left [p + A(j) right ]^2 %varphi
Current-DFT
V_xc , A_xc
i { partial } over { partial t} %varphi = (T+ V_h + V_xc + V_ext) %varphi
TD-DFT
V_xc
HARD

---
Linear Response Regime (I)
The external potential “induces” a (time-dependent) density perturbation
%chi(vec r t,{vec r}^{'} t^{'})= { %delta %rho^{ind}(r,t) } over { %delta %varphi _{ext} (r',t') } = - i langle [ %delta %rho(r,t) %delta %rho(r' t') ] rangle
Kubo Formula (1957)

---
Linear Response Regime (II)
%chi(vec r t,{vec r}^{'} t^{'})= %chi_0 (vec r t,{vec r}^{'} t^{'}) + int int dt_1 dt_2 int int d {vec r_1} d {vec r_2} %chi_0 (vec r t,{vec r_1} t_1) v({vec r_1}-{vec r_2})%chi({vec r_2}t_2 ,{vec r}^{'}t^{'})
Variation of the charge density w.r.t. the total potential.
%chi_0 ({vec r},{vec r}^{'}) = { %delta %rho_{ind}(vec r, t) } over { V_{tot}({vec r}^{'} t^{'}) }
+
=
+
+
=
+ ...
V_{tot}(vec r t)= V_{ext}(vec r t) + int dt' int d {vec r}^{'} v(vec r-{vec r}^{'}) %rho_{ind}({vec r}^{'} t^{'})
The induced charge density results in a total potential via the Poisson equation.
%chi (r,r',t-t') = { %delta %rho(r,t) } over { %delta V_{ext} (r',t')} = { %delta %rho(r,t) } over { %delta V_{tot} (r'',t'')} { %delta V_{tot}(r'',t'') } over { %delta V_{ext} (r',t')}
Screening of the external perturbation
Kubo Formula
%rho_{ind} V_{ind} V_{tot}

---
Linear Response Regime (III)
The screening is described by the inverse of the microscopic dielectric function
%epsilon^{-1}(vec r t,{vec r}^{'}t^{'})= {%delta V_{tot}(vec r t)} over {%delta V_{ext}(vec r t)}
{} = %delta(vec r - {vec r}^{'})+int dt^{''} d {vec r}^{''} v(vec r-{vec r}^{''}) %chi({vec r}^{''},{vec r}^{'})
Twofold physical meaning :
The convolution integrals in real space can be reduced to products is Fourier space
%epsilon^{-1}_{bold G bold G'}(bold q, %omega) = 1 + v_{bold G}(bold q) %chi_{bold G bold G'}(bold q, %omega)
bold G = bold G' = 0
Microscopic level: screening of the interaction between charge carriers in the system
In the long wave length limit it determines the macroscopic dielectric function which gives rise to screening of the external perturbation

---
Optical Absorption: Time Dependent DFT
V_eff(bold r , t) = V_{H} (bold r , t) + V_{xc} (bold r , t) + V_{ext} (bold r , t)
Petersilka et al. Int. J. Quantum Chem. 80, 584 (1996)
... by using ...
%delta %rho_I = %delta %rho_{"NI"}
%chi %delta V_{ext} = %chi^{0} (%delta V_{ext}+%delta V_{H}+%delta V_{xc})
TDDFT is an exact theory for neutral excitations!
%chi(bold q , %omega) = %chi^{0}(bold q , %omega) + %chi^{0}(bold q , %omega) (v +f_{xc}(bold q , %omega)) %chi(bold q , %omega)
Interacting System
Non Interacting System
[-{{1} over {2}} nabla^{2} + V_eff(bold r , t)] %psi_i(bold r , t) = i {partial } over {partial t} %psi_i(bold r , t) %rho(bold r , t) = Sum from {i = 1} to {N} lline %psi_i(bold r , t) rline^2
%chi = {%delta %rho_I} over {%delta V_{ext}} %chi_0 = {%delta %rho_{"NI"}} over {%delta V_{eff}}
%chi = %chi^{0} (1 + {%delta V_{H}} over {%delta V_{ext}}+{%delta V_{xc}} over {%delta V_{ext}}) v %chi f_{xc} %chi

---
Why does paper turn yellow?
Treasure map
By comparing ultraviolet-visible reflectance spectra of ancient and artificially aged modern papers with ab-initio TD-DFT calculations, it was possible to identify and estimate the abundance of oxidized functional groups acting as chromophores and responsible of paper yellowing.
A. Mosca Conte et al.,
Phys. Rev. Lett. 108, 158301 (2012)

---
Optical Absorption: Microscopic View (II)
e
Elementary process of absorption: Photon creates a single e-h pair
h
W = {2 %pi} over {hbar} Sum from{i,j} lline langle %phi_i mline bold e cdot bold hat v mline %phi_j rangle rline^{2} %delta(%epsilon_i-%epsilon_j - hbar %omega) sim Im {%epsilon(%omega)}
   Non Interacting quasi-particles
%epsilon_i, %epsilon_j
%epsilon_i, %epsilon_j
GW corrected energies
Hartree, HF, DFT
Independent transitions
Non Interacting Particles

---
Optical Absorption: Microscopic View (III)
Direct and indirect interactions between an e-h pair created by a photon
 Summing up all such interaction processes we get:
L(bold r_1 t_1;bold r_2 t_2; bold r_3 t_3; bold r_4 t_4) = L(1,2,3,4)
The equation for L is the Bethe Salpeter Equation. The poles are the neutral excitations.

---
Derivation of the Bethe-Salpeter equation (1)
V(1) = U(1) -i hbar int d3 v(1,3) %rho (3)
... by using ...
%epsilon^{-1}(1,2) = %delta(1,2) + int d3 v(1,3) {langle %delta %rho(3) rangle } over {%delta U(2)}
i=bold r_i,t_i
The density is related
to the Green's function by
langle %rho(1) rangle = -i hbar G(1, 1^{ {} + {} })
G_2(1, 3; 2, 3^{ {} + {} } ) = G(1,2)G(3,3^{ {} + {} }) - { %delta G(1,2) } over { %delta U(3)}
... by the identity ...
Reducible polarizability
%chi(1,2) = { %delta langle %rho (1) rangle } over { %delta U (2) } = i hbar [G_2(1, 2; 1^{ {} + {} }, 2^{ {} + {} } ) - G(1,1 ^{ {} + {} })G(2,2^{ {} + {} }) ]
two-particle correlation function
%chi(1,2) = - i hbar color green { L(1, 2; 1^{"+"}, 2^{"+"} ) }
G. Strinati, Rivista del Nuovo Cimento, 11, 1 (1988)
%epsilon^{-1}(1,2)={%delta V(1) } over {%delta U(2)}
What we want:

---
Derivation of the Bethe-Salpeter equation (2)
What we have:
What we have:
Dyson equation
[ i hbar {partial } over {partial t} - h(1) - U(1) ] G(1,2) - int { d4 %SIGMA(3,4) G(4,2) } = %delta(1,2)
%chi(1,2) = -i { %delta langle G(1,1^{ {} + {} } ) rangle } over { %delta U (2) } = { %delta langle %rho(1) rangle } over { %delta U (2) } = langle %delta %rho(1) %delta %rho(2) rangle
Using:
{ %delta G(1,4) } over { %delta U (5,6) } = L(1,5,4,6) = - int G (1,2) { %delta G^{-1}(2,3) }over { %delta U (5,6) } G (3,4)
G^{-1}(1,2) = G^{(0) -1} (1,2) - U(1)%delta(1,2) - %SIGMA(1,2)
Just the Dyson equation for G-1

---
Derivation of the Bethe-Salpeter equation (3)
L^0(1,2,3,4) = G(1,4)G(2,3)
Coulomb term
%SIGMA(1, 2) = G(1,2)v(2,1)
=> Time-Dependent Hartree-Fock
Screened Coulomb term
=> Standard Bethe-Salpeter equation
(Time-Dependent Screened Hartree-Fock)
%SIGMA^{GW}(1, 2) = −iG(1,2)W(2,1)
L = L_0 + L_0 [ v − {%delta (G W)} over {%delta G}] L
L = L_0 + L_0 [v + {%delta %SIGMA} over {%delta G}] L
Bethe-Salpeter Equation!

---
Feynman's diagrams and
Bethe-Salpeter equation
Intrinsc 4-point equation.
It describes the (coupled) progation of
two particles, the electron and the hole !
Retardation effects are neglected
W(1,2) = W(bold r_1 , bold r_2) %delta(t_1 ,t_2)
L(1,2,3,4) = L(bold r_1, bold r_2, bold r_3, bold r_4; t − t_0) = L(1,2,3,4, %omega)
L(1234) = L_0(1234)+ {} {} + L_0(1256) [v(57) color red {%delta(56) %delta(78)} −W(56) color red {%delta(57) %delta(68)}] L(7834)
Quasihole and quasielectron
L = L_0 + L_0 [v − W] L
+
-
=

---
Bethe-Salpeter equation (4-points - space and time)
L(1,2,3,4) = L(bold r_1, bold r_2, bold r_3, bold r_4; t − t_0) = L(1,2,3,4, %omega)
Should we invert the equation for L for each frequency???
We work in transition space...
-
+
-
+
-
+
H^{exc}_{(n_1 n_2),(n_3 n_4)} A_{%lambda}^{(n_3 n_4)} = E_{%lambda} A_{%lambda}^{(n_1 n_2)}

---
Effective two particle Hamiltonian
It corresponds to transitions at positive absorption frequencies
v .
It corresponds to transitions at negative absorption frequencies
v .
Tamm Dancoff!!!
%epsilon_M(%omega) = 1 - lim from {bold q rightarrow 0} v(bold q) Sum from {%lambda} sum from {vc, bold k} { lline langle v bold { k-q } lline e^{ - i bold q bold r} rline c bold{k }rangle rline^2 } over { E_{%lambda} -%omega - i %eta}
Pseudo-Hermitian

---
Bethe Salpeter Equation Historical remarks…
First solution of BSE
with dynamical effects: Shindo approximation
JPSJ 29, 278(1970)
Plane-waves implementation
G. Onida et al.
PRL 75, 818 (1995)
First applications in solids:
 W. Hanke and L.J. Sham PRL 33, 582(1974)
 G. Strinati, H.J. Mattausch and W. Hanke
PRL 45, 290 (1980)
1951
1970
1974
1995

---
… Some results …
Bruneval et al., PRL 97, 267601 (2006)
Strinati et al., Rivista del Nuovo Cimento 11, 1 (1988)
Albrecht et al., PRL 80, 4510
(1998)
Bruno et al., PRL 98, 036807 (2007)
V. Garbuio et al., PRL 97, 137402 (2006)
Tiago et al., PRB 70, 193204 (2004)

---
Excitons in nanoscale systems
Nanotubes/Nanowires
Frenkel excitons in photosynthesis
Colloidal quantum dots
Excitons in nanoscale systems
Gregory D. Scholes, Garry Rumbles
Nature Materials 5, 683 - 696 (2006)
[Speaker Notes: The yellowing of paper on aging causes major aesthetic damages of cultural heritage. It is due to cellulose oxidation, a complex process with many possible products still to be clarified. By comparing ultraviolet-visible reflectance spectra of ancient and artificially aged modern papers with ab initio time- dependent density functional theory calculations, we identify and estimate the abundance of oxidized functional groups acting as chromophores and responsible of paper yellowing. This knowledge can be used to set up strategies and selective chemical treatments preventing paper yellowing.]

---
. . . advances . . .
[Speaker Notes: The yellowing of paper on aging causes major aesthetic damages of cultural heritage. It is due to cellulose oxidation, a complex process with many possible products still to be clarified. By comparing ultraviolet-visible reflectance spectra of ancient and artificially aged modern papers with ab initio time- dependent density functional theory calculations, we identify and estimate the abundance of oxidized functional groups acting as chromophores and responsible of paper yellowing. This knowledge can be used to set up strategies and selective chemical treatments preventing paper yellowing.]

---
Beyond Tamm-Dancoff approximation!
Mixed excitonic-plasmonic excitations
in nanostructures (Nanoletters, 6, 257(2010))
Excited states of biological chromophores (J. Chem. Theory Comput., 6, 257–265 (2010))
[Speaker Notes: Nanotube In this work, we argue that for confined systems, such as nanotubes or π-conjugated molecules, the excitations appearing in the response function show a mixed excitonic-plasmonic behavior. As a consequence the e-h pair-antipair interaction becomes crucial and the TDA does not hold anymore. A paradigmatic example is the trans-azobenzene molecule, where the TDA overestimates the position of the main peak in the polarizability spectrum by ∼0.2 eV. Even more intriguing is the case of carbon nanotubes that, because of the quasi-one-dimensional (1D) structure, behave either as extended or isolated system depending on the polarization of the perturbing field. Thus, for transverse perturbations the excitons acquire a plasmonic nature and the TDA overestimates the position of the π plasmon peak appearing in both absorption and EEL spectra by almost 1 eV. Chromophores: Chromophores are quasi-zero-dimensional systems. The distribution of the excited electron and the hole is highly localized. It is the huge exchange interaction between the excited electron and the hole that makes the resonant-anti- resonant coupling not negligible. When the dimension of the system increases, such as in polymers, nanotubes, and bulk solids, the excited electron and hole becomes delocalized and the influence of TDA decreases gradually. We also include dynamical screening effects in the electron-hole interaction. In comparison to the results from calculations with only static screening, we find that the influence of dynamical screening on the excitation energies is about 0.1 eV for the lowest π f π* transitions, but for the lowest n f π* transitions the influence is larger, up to 0.25 eV.]

---
Ab-initio broadening in BSE
Ab-Initio finite temperature
 excitons
A. Marini PRL 101, 106405 (2008).
Ab Initio Calculation of Optical Spectra of Liquids: Many-Body Effects in the Electronic Excitations of Water
V. Garbuio et al.,
PRL 97, 137402(2006).

---
Dynamical Excitonic Effects in Metals and Semiconductors
The inclusion of the full dynamic screening in the BS equation complicates its numerical solution tremendously, but it is possible to perform an expansion in the dynamical part of the screened interaction. First solution of this problem the so-called
Shindo approximation (J. Phys. Soc. Jpn. 29, 278(1970))
Dynamical effects in Sodium clusters
G. Pal et al.
EPJ B 79, 327 (2011)
Dynamical effects
in metals and semiconductors
A. Marini and R. Del sole
PRL, 91, 176402 (2003).
[Speaker Notes: The numerical calculations needed for these Bethe-Salpeter approaches are simplified if one assumes an instantaneous, i.e., statically screened, electron-hole interaction for the direct part of the integral kernel of the BS equation. This approach works quite well in a few extended systems, such as semiconductors and insulators. The straightforward inclusion of the full dynamic screening in the BS equation complicates its numerical solution tremendously, but it is possible to perform an expansion of the dynamically screened potential in plasmonic modes. Dynamic screening is also responsible for excitonic effects even in metals, such as Cu and Ag6. General attacks on the problem of dynamic screening in the BS equation go back to the Shindo approximation. More recently this problem has been reexamined in the framework of nonequilibrium Green function theory, which allows one to derive a Dyson equation for the two-particle propagator.]

---
Non-linear response:
frequency and time domain
Second-order response Bethe-Salpeter equation (PRA, 83, 062122 (2011))
Second-order response Bethe-Salpeter equation (PRA, 83, 062122 (2011))
Real-time approach to the optical properties of solids and nanostructures: Time-dependent Bethe-Salpeter equation
(PRB, 84, 245110 (2011))

---
References!!!
Reviews:
Application of the Green’s functions method to the study of
the optical properties of semiconductors
Nuovo Cimento, vol 11, pg 1, (1988) G. Strinati
Effects of the Electron–Hole Interaction on the Optical Properties
of Materials: the Bethe–Salpeter Equation
Physica Scripta, vol 109, pg 141, (2004) G. Bussi
Electronic excitations: density-functional versus many-body
 Green's-function approaches
RMP, vol 74, pg 601, (2002	) G. Onida, L. Reining, and A. Rubio
Books:
On the web:
http://yambo-code.org/lectures.php
http://freescience.info/manybody.php
http://freescience.info/tddft.php
http://freescience.info/spectroscopy.php

---
DFT meets Many-Body

---
….. with some algebra......

---
References!!!
Reviews:
Application of the Green’s functions method to the study of
the optical properties of semiconductors
Nuovo Cimento, vol 11, pg 1, (1988) G. Strinati
Effects of the Electron–Hole Interaction on the Optical Properties
of Materials: the Bethe–Salpeter Equation
Physica Scripta, vol 109, pg 141, (2004) G. Bussi
Electronic excitations: density-functional versus many-body
 Green's-function approaches
RMP, vol 74, pg 601, (2002	) G. Onida, L. Reining, and A. Rubio
Books:
On the web:
http://yambo-code.org/lectures.php
http://freescience.info/manybody.php
http://freescience.info/tddft.php
http://freescience.info/spectroscopy.php

---
Optical Absorption: Microscopic Limit
%chi^{0} = Sum from{ij} {{ %phi_i(bold r) %phi_j^{"*"}(bold r) %phi_i^{"*"}(bold r') %phi_j(bold r')} over {%omega - (%epsilon_i-%epsilon_j) +i%eta} }
%delta %rho_{"NI"} = %chi^{0} %delta V_{tot}
Hartree, Hartree-Fock, dft...
Absorption by independent
Kohn-Sham particles
{} = Im %chi_0 = Sum from{ij} lline langle j mline D mline i rangle rline^{2} %delta (%omega - ( %epsilon_j − %epsilon_i ))
%epsilon^{"''"}(%omega) = {8%pi^{2}} over {%omega^2} Sum from{i,j} lline langle %phi_i mline bold e cdot bold hat v mline %phi_j rangle rline^{2} %delta(%epsilon_i-%epsilon_j - hbar %omega)
Particles are interacting!
Non Interacting System