Invisible excitations
in hexagonal Boron Nitride
Claudio Attaccalite

---
Outline
- h-BN introduction
- Indirect excitations
  - EELS
  - Exciton interference
- Dark excitons in bulk h-BN
  - Origin
  - Non-linear spectroscopy
- Conclusions: excitons and luminescence

---
Hexagonal Boron Nitride
h-BN is a layered
crystal homo-structural to graphite.
As graphite, h-BN can be easily exfoliated, and for this reason it finds applications as lubricant .

---
Hexagonal Boron Nitride
h-BN has a large band gap and its transparent
h-BN emits light in the ultraviolet

---
Breaking news
on h-BN !!!
Direct-bandgap properties and evidence for ultraviolet lasing of h-BN single crystal
K. Watanabe et al. Nature Materials 3, 404 (2004)*

---
Breaking news
on h-BN !!!
Direct-bandgap properties and evidence for ultraviolet lasing of h-BN single crystal
K. Watanabe et al. Nature Materials 3, 404 (2004)*
Hexagonal boron nitride is an indirect band-gap semiconductor
G. Cassabois et al., Nature Photonics, 10, 262 (2016)*
*) results from Luminescence measurements

---
h-BN band structure

---
How to probe h-BN
beyond luminescence

---
h-BN band structure and ARPES

---
h-BN optical properties

---
h-BN optical properties
Excitons in boron nitride nanotubes: dimensionality effects
Phys. Rev. Lett. 96, 126104 (2016)

---
Electron loss spectroscopy on h-BN

---
Theory: how to calculate e(w)
Excitons in boron nitride single layer
T. Galvani et al., Phys. Rev. B 94, 125303 (2016)
G. Strinati, Nuovo Cimento 11, 1 (1988)

---
Theory vs experiments
Angular resolved electron energy loss spectroscopy in hexagonal boron nitride
F. Fossard et al. Phys. Rev. B 96 115304 (2017)

---
May we probe indirect nature of h-BN with EELS?

---
Theoretical results on EELS
Exciton interference in hexagonal boron nitride
L. Sponza, et al.
arXiv preprint arXiv:1709.07397

---
Origin of the EELS peaks
Loss function
 Peaks of L(q, ω) can be put in relation to inter-band excitations (∝ Im[ε(q, ω)])
and plasmon resonances (|ε| ≈ 0)
Exciton interference in hexagonal boron nitride
L. Sponza, H. Amara, C. Attaccalite, F. Ducastelle, A. Loiseau
arXiv preprint arXiv:1709.07397

---
Origin of the EELS peaks
Loss function
 Peaks of L(q, ω) can be put in relation to inter-band excitations (∝ Im[ε(q, ω)])
and plasmon resonances (|ε| ≈ 0)
Exciton interference in hexagonal boron nitride
L. Sponza, H. Amara, C. Attaccalite, F. Ducastelle, A. Loiseau
Physical Review B 97 (7), 075121 (2018)

---
May we probe indirect nature of h-BN with EELS?
Direct Observation of the Lowest Indirect Exciton State in the Bulk
of Hexagonal Boron Nitride
R. Schuster C. Habenicht, M. Ahmad, M. Knupfer, B. Büchner, PRB 97, 041201 (2018)

---
Theory vs Experiment

---
Origin of peak intensity
 The contribution from K→M and M→ K’
has opposite sign
 When they have the same intensity the exciton is dark otherwise is bright

---
Origin of peak intensity

---
Excitons analysis q=0.7A
The strength of the peak is explained by the fact that the KM transitions take place between regions of the band structure where bands are particularly, from top valence to the M point.
Positive
Negative

---
Excitons analysis q=1.12A
At this q point the contribution from K→M and M→ K’ is of the same order but with opposite sign, therefore the exciton is dark.
Positive
Negative

---
Conclusions {at finite momentum}
- Indirect nature of h-BN can be probed by EELS
- Peaks intensity in EELS originates from constructive/destructive sum of finite momentum transition between M→K and K→M
- Theory explains recent experiments on h-BN at finite momentum

---
Invisible excitons at zero momentum (2n part)
INVISIBLE EXCITONS
        Not, but I’m invisible
        like you
        do you
 have a finite momentum?

---
Nature of excitons in single-layer h-BN
 Schematic splitting scheme of the 2p levels.
(Lowest states are degenerate,
one bright and one dark)
 Tight-binding amplitudes for the two degenerate states, symmetric and antisymmetric with respect to the y-axis.
Excitons in boron nitride single layer
T. Galvani et al., Phys. Rev. B 94, 125303 (2016)

---
Nature of excitons in bulk h-BN
Combinations with respect to the exchange of the e-h pair between two inequivalent layers
Third and fourth excitons
Splitting due to the
interlayer hopping
The two lowest excitons
Excitons in van der Waals materials: From monolayer to bulk hexagonal boron nitride
J. Koskelo, et al, Phys. Rev. B 95, 035125 (2017)

---
How to probe dark states at q=0?

---
Non-linear response can probe
dark states due to
the different selection rules!!!
P(r,t) = %chi^{(1)} E + %chi^{(2)} E^2 + color red {%chi^{(3)} E^3} + O(E^4)

---
How to calculate non-linear response in h-BN
 Nonlinear optics from an ab-initio approach by means of the dynamical Berry phase
Attaccalite, C., & Grüning, M.
PRB, 88(23), 235113. (2013)

---
TPA coefficients
from real-time simulations
  Real-time dynamics
  Real-time dynamics

---
TPA coefficients
from real-time simulations
  Real-time dynamics
  Real-time dynamics
Polarization

---
TPA coefficients
from real-time simulations
  Real-time dynamics
  Real-time dynamics
Polarization
Richardson
extrapolation

---
TPA coefficients
from real-time simulations
  Real-time dynamics
  Real-time dynamics
Polarization
Richardson
extrapolation

---
Two-photon absorption
Monolayer h-BN
Two-photons absorption in hexagonal boron nitride
C. Attaccalite et al., unpublished

---
Two-photon absorption
Monolayer h-BN
Bulk h-BN
Two-photons absorption in hexagonal boron nitride
C. Attaccalite et al., arXiv preprint arXiv:1803.10959

---
Tight-binding modeling 1/2
Monolayer h-BN
also that all excitons are in principle bright. We have seen in particular that the oscillator strength for the ground state 1s exciton is very strong.
1 - Photon
The excitonic states can then be classified according to the representations of the C3v point group.
Among the three representations A1, A2 and E, only the two-dimensional representation E is optically active.
2 - Photon
 In the discrete which indicates

---
Experimental results
Probing the 1s state in WS2
explanation in terms
of magnetic dipoles
Giant Enhancement of the Optical Second-Harmonic Emission of WSe2 Monolayers by Laser Excitation at Exciton Resonances
Phys. Rev. Lett. 114, 097403 (2015)

---
Experimental results
Hexagonal boron nitride is an indirect band-gap semiconductor
G. Cassabois et al., Nature Photonics, 10, 262 (2016)

---
Experimental results
Hexagonal boron nitride is an indirect band-gap semiconductor
G. Cassabois et al., Nature Photonics, 10, 262 (2016)

---
Conclusions {at zero momentum}
- Two-photon absorption can probe 1s excitons with in two-dimensional crystals
- Dark excitons in bulk h-BN not visible in absorption can be probed by two-photon absorption
- Dark excitons have too high energy at zero momentum, but at finite q they produce the double peaks structures

---
Conclusions
Using a combinations of different spectroscopic techniques all excited states of h-BN can be found!!!
References
Exciton interference in hexagonal boron nitride
L. Sponza, H. Amara, C. Attaccalite, F. Ducastelle, A. Loiseau
Phys. Rev. B 97, 075121 (2017)
Angle-resolved electron energy loss spectroscopy in h-BN
F. Fossard, et al.
Phys. Rev. B 96, 115304 (2017)
 Two-photons absorption in hexagonal boron nitride
C. Attaccalite et al., arXiv preprint arXiv:1803.10959
Lumen code for the non-linear response (GPL)
http://www.attaccalite.com/lumen/
This presentation is available on: http://attaccalite.com

---
Acknowledgments
Hakim Amara
Myrta Grüning
François Ducastelle
Lorenzo Sponza
 Annick Loiseau
Frédéric Fossard
Léonard Schué