Invisible excitons
in hexagonal Boron Nitride
Claudio Attaccalite

---
Outline
- h-BN introduction
- Indirect excitons
  - EELS
  - Exciton interference
- Dark excitons in bulk h-BN
  - Origin
  - Non-linear spectroscopy
- Conclusions: excitons and luminescence

---
Hexagonal Boron Nitride
h-BN is a layered
crystal homo-structural to graphite.
As graphite, h-BN can be easily exfoliated, and for this reason it finds applications as lubricant .

---
Hexagonal Boron Nitride
h-BN has a large band gap and its transparent
h-BN emits light in the ultraviolet

---
Breaking news
on h-BN !!!
Direct-bandgap properties and evidence for ultraviolet lasing of h-BN single crystal
K. Watanabe et al. Nature Materials 3, 404 (2004)*

---
Breaking news
on h-BN !!!
Direct-bandgap properties and evidence for ultraviolet lasing of h-BN single crystal
K. Watanabe et al. Nature Materials 3, 404 (2004)*
Hexagonal boron nitride is an indirect band-gap semiconductor
G. Cassabois et al., Nature Photonics, 10, 262 (2016)*
*) results from Luminescence measurements

---
h-BN band structure

---
How to probe h-BN
beyond luminescence

---
h-BN band structure and ARPES

---
Electron loss spectroscopy on h-BN

---
Theory: how to calculate e(w)
Excitons in boron nitride single layer
T. Galvani et al., Phys. Rev. B 94, 125303 (2016)
G. Strinati, Nuovo Cimento 11, 1 (1988)

---
Theory vs experiments
Angular resolved electron energy loss spectroscopy in hexagonal boron nitride
F. Fossard et al. Phys. Rev. B 96 115304 (2017)

---
May we probe indirect nature of h-BN with EELS?
Direct Observation of the Lowest Indirect Exciton State in the Bulk
of Hexagonal Boron Nitride
R. Schuster et al. arXiv:1706.04806

---
EELS - theory and experiments
Exciton interference in hexagonal boron nitride
L. Sponza, et al.
arXiv preprint arXiv:1709.07397

---
Origin of the EELS peaks
Loss function
 Peaks of L(q, ω) can be put in relation to inter-band excitations (∝ Im[ε(q, ω)])
and plasmon resonances (|ε| ≈ 0)
Exciton interference in hexagonal boron nitride
L. Sponza, H. Amara, C. Attaccalite, F. Ducastelle, A. Loiseau
arXiv preprint arXiv:1709.07397

---
Origin of the EELS peaks
Loss function
 Peaks of L(q, ω) can be put in relation to inter-band excitations (∝ Im[ε(q, ω)])
and plasmon resonances (|ε| ≈ 0)
Exciton interference in hexagonal boron nitride
L. Sponza, H. Amara, C. Attaccalite, F. Ducastelle, A. Loiseau
arXiv preprint arXiv:1709.07397

---
Origin of peak intensity

---
Excitons analysis q=0.7A
The strength of the peak is explained by the fact that the KM transitions take place between regions of the band structure where bands are particularly, from top valence to the M point.
Positive
Negative

---
Excitons analysis q=1.12A
At this q point the contribution from K→M and M→ K’ is of the same order but with opposite sign, therefore the exciton is dark.
Positive
Negative

---
Conclusions {at finite momentum}
- Indirect nature of h-BN can be probed by EELS
- Peaks intensity in EELS originates from constructive/destructive of finite momentum transition between M→K and K→M
- Theory explains recent experiments on h-BN at finite momentum

---
Invisible excitons at zero momentum (2n part)
INVISIBLE EXCITONS
        Not, but I’m invisible
        like you
        do you
 have a finite momentum?

---
Nature of excitons in single-layer h-BN
 Schematic splitting scheme of the 2p levels.
(Lowest states are degenerate,
one bright and one dark)
 Tight-binding amplitudes for the two degenerate states, symmetric and antisymmetric with respect to the y-axis.
Excitons in boron nitride single layer
T. Galvani et al., Phys. Rev. B 94, 125303 (2016)

---
Nature of excitons in bulk h-BN
Combinations with respect to the exchange of the e-h pair between two inequivalent layers
Third and fourth excitons
Splitting due to the
interlayer hopping
The two lowest excitons
Excitons in van der Waals materials: From monolayer to bulk hexagonal boron nitride
J. Koskelo, et al, Phys. Rev. B 95, 035125 (2017)

---
Two-photon absorption
Monolayer h-BN
Two-photons absorption in hexagonal boron nitride
C. Attaccalite et al., unpublished

---
Two-photon absorption
Monolayer h-BN
Bulk h-BN
Two-photons absorption in hexagonal boron nitride
C. Attaccalite et al., unpublished

---
Conclusions {at zero momentum}
- Dark excitons not visible in absorption and luminescence can be probed by two-photon absorption
- Two-photon absorption can probe excitons with different selection roles in two-dimensional crystals

---
Conclusions {at zero momentum}
- Dark excitons not visible in absorption and luminescence can be probed by two-photon absorption
- Two-photon absorption can probe excitons with different selection rules in two-dimensional crystals
Conclusions
Using a combinations of different spectroscopic techniques all excited states of h-BN have been finally found!!!

---
Acknowledgments
Hakim Amara
Myrta Grüning
François Ducastelle
Lorenzo Sponza
 Annick Loiseau
Frédéric Fossard
Léonard Schué

---
References
Exciton interference in hexagonal boron nitride
L. Sponza, H. Amara, C. Attaccalite, F. Ducastelle, A. Loiseau
arXiv preprint arXiv:1709.07397
Angle-resolved electron energy loss spectroscopy in h-BN
F. Fossard, et al.
Phys. Rev. B 96, 115304 (2017)
 Two-photons absorption in hexagonal boron nitride
C. Attaccalite et al., unpublished
Lumen code for the non-linear response (GPL)
http://www.attaccalite.com/lumen/

---
TPA coefficients
from real-time simulations
  Real-time
dynamics
Richardson
extrapolation