Bethe-Salpeter Equation
Time-dependent approach
Claudio Attaccalite
http://attaccalite.com
[Speaker Notes: In an experiment like optical absorption we explore the probability of creating neutral excitations – no particle added or removed from the system -> optical gap]

---
Beyond the independent-particle picture
Time-dependent Hartree plus screened exchange
The Bethe-Salpeter equation

---
Summary of the earlier episodes
1) Chose a single-particle Hamiltonian
H⁰, H^{ Hartree }, H^{ DFT }, etc...
i { partial {hat %rho}(t) } over { partial t} = [ H, {hat %rho} ] %chi(vec r t,{vec r}^{'} t^{'})= { %delta %rho^{ind}(r,t) } over { %delta V _{tot} (r',t') }
2) Derive the corresponding c(w)
 using Von Neumann equation
3) The G0W0 approximation improve
the KS band structure

---
Including everything in
an Hamiltonian formalism
%DELTA_i^{G_0 W_0} = %epsilon_i^{ GoWo } - %epsilon_i^{ DFT }
H_{GoWo} = H + sum_i left none {} mline %phi_i right rangle left langle %phi_i mline {} right none %DELTA_i^{ G_0 W_0 }
Lithium fluoride
Let’s do a DFT+GW calculation:
Completely wrong!
Presence of below band gap excitations!
[Speaker Notes: \mathrm{Abs}(\omega) \propto \sum_{cvk} \  D_{cvk}^2  \ \delta (\omega -[E_{ck}-E_{vk}])]

---
Going beyond the independent-particle picture
We need to account for the electron-hole interaction
[Speaker Notes: \mathrm{Abs}(\omega) \propto \sum_{\textcolor{red}{\lambda}} \biggl\lvert \sum_{cvk} \ \textcolor{red}{A_{\lambda}^{cvk}} \ D_{cvk} \biggr\rvert^2 \ \delta (\omega -\textcolor{red}{E_\lambda})]

---
Going beyond the independent-particle picture
We need to account for the electron-hole interaction
[Speaker Notes: \mathrm{Abs}(\omega) \propto \sum_{\textcolor{red}{\lambda}} \biggl\lvert \sum_{cvk} \ \textcolor{red}{A_{\lambda}^{cvk}} \ D_{cvk} \biggr\rvert^2 \ \delta (\omega -\textcolor{red}{E_\lambda})]

---
Going beyond the independent-particle picture
Especially relevant to layered/2D materials
DFT+GW
Hexagonal boron nitride
y
x
DFT+GW+BSE
z
x
Band gap
Band gap
[Speaker Notes: \mathrm{Abs}(\omega) \propto \sum_{\textcolor{red}{\lambda}} \biggl\lvert \sum_{cvk} \ \textcolor{red}{A_{\lambda}^{cvk}} \ d_{cvk} \biggr\rvert^2 \ \delta (\omega -\textcolor{red}{E_\lambda})]

---
Going beyond the independent-particle picture
Especially relevant to layered/2D materials
DFT+GW
Hexagonal boron nitride
y
x
DFT+GW+BSE
z
x
Band gap
Band gap
[Speaker Notes: \mathrm{Abs}(\omega) \propto \sum_{\textcolor{red}{\lambda}} \biggl\lvert \sum_{cvk} \ \textcolor{red}{A_{\lambda}^{cvk}} \ d_{cvk} \biggr\rvert^2 \ \delta (\omega -\textcolor{red}{E_\lambda})]

---
How can we derive the BSE?
Real-time dynamics of the response function
Iteration of Hedin’s equations that contain the response function
HEDIN
SCHWINGER
G. Strinati, Riv. Nuovo Cim. 11, 12 (1988)
Generalization of the response function to 4-point…
REAL TIME
[Speaker Notes: \chi(12)=\frac{\delta \rho(1)}{\delta V_{\mathrm{ext}}(2)} \rightarrow \prescript{4}{}L(1234)=\frac{\delta G(12)}{\delta V_{\mathrm{ext}(34)}} \chi(12)=\frac{\delta \rho(1)}{\delta V_{\mathrm{ext}}(2)} \rightarrow \mathrm{i} \frac{\partial \chi(12)}{\partial t}=\dots]

---
How can we derive the BSE?
Real-time dynamics of the response function
Iteration of Hedin’s equations that contain the response function
HEDIN
SCHWINGER
G. Strinati, Riv. Nuovo Cim. 11, 12 (1988)
Generalization of the response function to 4-point…
REAL TIME
[Speaker Notes: \chi(12)=\frac{\delta \rho(1)}{\delta V_{\mathrm{ext}}(2)} \rightarrow \prescript{4}{}L(1234)=\frac{\delta G(12)}{\delta V_{\mathrm{ext}(34)}} \chi(12)=\frac{\delta \rho(1)}{\delta V_{\mathrm{ext}}(2)} \rightarrow \mathrm{i} \frac{\partial \chi(12)}{\partial t}=\dots]

---
Choosing a description for the electronic system
Single-particle Hamiltonian from Hartree-Fock
{hat H}_{HF} (t) = T_e + V_{ e -N } + V_H [ %rho] + %SIGMA^{x} [ {hat %rho} ]
where
[Speaker Notes: \rho^0 is diagonal in the Bloch states and time-independent]

---
Time-dependent Hartree-Fock
Full Hamiltonian
TD-Hartree
TD-exchange
H0HF at equilibrium
{hat H}_{HF} (t) = T_e + V_{ e -N } + V_H [ %rho^0] + %SIGMA^{x} [ {hat %rho} ^0]
[Speaker Notes: \Delta\hat{V}^H [\rho(t)]=\hat{V}^H[\rho(t)]-\hat{V}^H[\rho^0]]

---
Time-dependent Hartree-Fock
Full Hamiltonian
TD-Hartree
TD-exchange
These term will generate electron-hole interaction and bound states in the gap!!!
H0HF at equilibrium
{hat H}_{HF} (t) = T_e + V_{ e -N } + V_H [ %rho^0] + %SIGMA^{x} [ {hat %rho} ^0]
[Speaker Notes: \Delta\hat{V}^H [\rho(t)]=\hat{V}^H[\rho(t)]-\hat{V}^H[\rho^0]]

---
A better Hamiltonian
H0GW+screened exchange
The Hamiltonian that generates the BSE
{hat H}_{BSE} (t) = H_{GW}^0 + %DELTA {hat V}^H + %DELTA { hat %SIGMA}^{sex} [ {hat %rho} ]
TD-Hartree
TD-screened exchange
%DELTA { hat %SIGMA}^{sex} [ {hat %rho}(t) ] = {hat %SIGMA}^{sex} [ {hat %rho}^0 ] -{hat %SIGMA}^{sex} [ {hat %rho}^0 ]
[Speaker Notes: \Delta\hat{V}^H [\rho(t)]=\hat{V}^H[\rho(t)]-\hat{V}^H[\rho^0]]

---
Equation of motion
For the density matrix:
For the response function (taking the functional derivative of the above):
The solution of this equation will yield the BSE!
[Speaker Notes: \mathrm{i}\frac{\partial}{\partial t}\chi_{\substack{n_1 n_2 \\ n_3 n_4}} (t,t^\prime) = \frac{\delta}{\delta U_{n_3 n_4}(t^\prime)} \left[ \hat{H}(t), \hat{\rho}(t)\right]_{n_1 n_2}]

---
Taking care of the two-particle kernel
Rewriting the density functionals
[Speaker Notes: \Delta V^H_{n_1 n_2} [\rho(t)] = \sum_{m_1 m_2}\int \mathrm{d} \overline{\overline{t}} \ \frac{ \delta V^H_{n_1 n_2}[\rho(t)]}{\delta U_{m_1 m_2} (\overline{\overline{t}})  } \ \delta U_{m_1 m_2} (\overline{\overline{t}})]

---
Taking care of the two-particle kernel
Rewriting the density functionals
[Speaker Notes: \Delta V^H_{n_1 n_2} [\rho(t)] = \sum_{m_1 m_2}\int \mathrm{d} \overline{\overline{t}} \ \frac{ \delta V^H_{n_1 n_2}[\rho(t)]}{\delta U_{m_1 m_2} (\overline{\overline{t}})  } \ \delta U_{m_1 m_2} (\overline{\overline{t}})]

---
Taking care of the two-particle kernel
Rewriting the density functionals
[Speaker Notes: \Delta V^H_{n_1 n_2} [\rho(t)] &= \sum_{m_1 m_2}\int \mathrm{d} \overline{\overline{t}} \ \frac{ \delta V^H_{n_1 n_2}[\rho(t)]}{\delta U_{m_1 m_2} (\overline{\overline{t}})  } \ \delta U_{m_1 m_2} (\overline{\overline{t}}) \\ &= \sum_{\substack{m_1 m_2 \\ m_2 m_4}} \int \mathrm{d} \overline{\overline{t}} \mathrm{d} \overline{t} \ \frac{ \delta V^H_{n_1 n_2}[\rho(t)]}{\delta \rho_{m_3 m_4} (\overline{t})  } \frac{ \delta\rho_{m_3 m_4}( \overline{t} )}{\delta U_{m_1 m_2} (\overline{\overline{t}})  }\ \delta U_{m_1 m_2} (\overline{\overline{t}})]

---
Taking care of the two-particle kernel
Rewriting the density functionals
By doing the same for
we obtain:
[Speaker Notes: \Delta V^H_{n_1 n_2} [\rho(t)] &= \sum_{m_1 m_2}\int \mathrm{d} \overline{\overline{t}} \ \frac{ \delta V^H_{n_1 n_2}[\rho(t)]}{\delta U_{m_1 m_2} (\overline{\overline{t}})  } \ \delta U_{m_1 m_2} (\overline{\overline{t}}) \\ &= \sum_{\substack{m_1 m_2 \\ m_2 m_4}} \int \mathrm{d} \overline{\overline{t}} \mathrm{d} \overline{t} \ \frac{ \delta V^H_{n_1 n_2}[\rho(t)]}{\delta \rho_{m_3 m_4} (\overline{t})  } \frac{ \delta\rho_{m_3 m_4}( \overline{t} )}{\delta U_{m_1 m_2} (\overline{\overline{t}})  }\ \delta U_{m_1 m_2} (\overline{\overline{t}})]

---
Taking care of the two-particle kernel
Rewriting the density functionals
Two-particle “kernel”
In order to proceed we will write down explicitly
and
and then compute the derivatives
[Speaker Notes: &\Delta V^H_{n_1 n_2} [\rho(t)] + \Delta \Sigma^x_{n_1 n_2} [\rho(t)] = \\ &= \sum_{\substack{m_1 m_2 \\ m_2 m_4}} \int \mathrm{d} \overline{\overline{t}} \mathrm{d} \overline{t} \ \left[ \frac{ \delta V^H_{n_1 n_2}[\rho(t)]}{\delta \rho_{m_3 m_4} (\overline{t})  } + \frac{ \delta \Sigma^x_{n_1 n_2}[\rho(t)]}{\delta \rho_{m_3 m_4} (\overline{t})  }\right] \chi_{\substack{m_3 m_4 \\ m_1 m_2 }}(\overline{t}, \overline{\overline{t}}) \ \delta U_{m_1 m_2} (\overline{\overline{t}})]

---
Time-dependent Hartree
[Speaker Notes: V^H_{n_1 n_2}(t) &= 2\sum_{l_1 l_2} \rho_{l_1 l_2} (t) \int \mathrm{d}^3r \,  \mathrm{d}^3 r^\prime  \ \varphi^*_{n_1}(\mathbf{r}) \varphi^*_{l_1}(\mathbf{r}^\prime) \varphi_{l_2}(\mathbf{r}^\prime)    \varphi_{n_2}(\mathbf{r}) \frac{1}{|\mathbf{r}-\mathbf{r}^\prime |}  \\ &\equiv 2\sum_{l_1 l_2} \rho_{l_1 l_2} (t) \, V_{\substack{n_1 n_2 \\ l_1 l_2}}]

---
Time-dependent Hartree
Momentum conservation implies that does not carry an internal momentum
[Speaker Notes: V^H_{n_1 n_2}(t) &= 2\sum_{l_1 l_2} \rho_{l_1 l_2} (t) \int \mathrm{d}^3r \,  \mathrm{d}^3 r^\prime  \ \varphi^*_{n_1}(\mathbf{r}) \varphi^*_{l_1}(\mathbf{r}^\prime) \varphi_{l_2}(\mathbf{r}^\prime)    \varphi_{n_2}(\mathbf{r}) \frac{1}{|\mathbf{r}-\mathbf{r}^\prime |}  \\ &\equiv 2\sum_{l_1 l_2} \rho_{l_1 l_2} (t) \, V_{\substack{n_1 n_2 \\ l_1 l_2}}]

---
Exchange (and correlation) self-energy
Time-dependent exchange
ISSUE: the unscreened Coulomb interaction overbinds electron and holes, giving wrong optical spectra.
[Speaker Notes: \Sigma^x_{n_1 n_2}(t) =- \sum_{l_1 l_2} \rho_{l_1 l_2} (t) \int \mathrm{d}^3r \, \mathrm{d}^3 r^\prime \ \varphi^*_{l_1}(\mathbf{r}^\prime) \varphi_{l_2}(\mathbf{r})\varphi^*_{n_1}(\mathbf{r}) \varphi_{n_2}(\mathbf{r}^\prime)\textcolor{blue}{v(\mathbf{r},\mathbf{r}^\prime)}]

---
Exchange (and correlation) self-energy
Time-dependent SEX
SOLUTION: we replace the Fock term with the statically screened exchange (SEX)
[Speaker Notes: \textcolor{red}{W(\mathbf{r},\mathbf{r}^\prime)}=\int \mathrm{d}^3 r^{\prime\prime}\varepsilon^{-1}_{\textcolor{red}{RPA}}(\mathbf{r},\mathbf{r}^{\prime\prime})v(\mathbf{r}^{\prime\prime},\mathbf{r})]

---
Exchange (and correlation) self-energy
Time-dependent SEX
SOLUTION: we replace the Fock term with the statically screened exchange (SEX)
NEGLECTED!
(Higher order in the interaction)
[Speaker Notes: \textcolor{red}{W(\mathbf{r},\mathbf{r}^\prime)}=\int \mathrm{d}^3 r^{\prime\prime}\varepsilon^{-1}_{\textcolor{red}{RPA}}(\mathbf{r},\mathbf{r}^{\prime\prime})v(\mathbf{r}^{\prime\prime},\mathbf{r})]

---
Solving the equation of motion (like in LR lecture)
A
B
C
[Speaker Notes: \mathrm{i}\frac{\partial}{\partial t}\chi_{\substack{n_1 n_2 \\ n_3 n_4}} (t,t^\prime) &= \frac{\delta}{\delta U_{n_3 n_4}(t^\prime)} \left[ \hat{H}^0(t), \hat{\rho}(t)\right]_{n_1 n_2} \\ &+ \frac{\delta}{\delta U_{n_3 n_4}(t^\prime)} \left[ \hat{U}(t), \hat{\rho}(t)\right]_{n_1 n_2} \\ &+ \frac{\delta}{\delta U_{n_3 n_4}(t^\prime)} \left[ -\sum_{\substack{m_1 m_2 \\ m_3 m_4}}\int \mathrm{d} \overline{\overline{t}}       \left( \hat{W}-2\hat{V} \right)  \chi^R_{\substack{m_3 m_4 \\ m_1 m_2}}\delta U_{m_1 m_2} (\overline{\overline{t}}), \hat{\rho}(t)\right]_{n_1 n_2}]

---
The Bethe-Salpeter equation
%chi_{ binom {n_1, n_2} {n_3, n_4} } ( %omega) = %chi^0_{ {n_1, n_2} } ( %omega) %delta_{n_1,n_3} %delta_{n_3, n_4} + %chi^0_{n_1, n_2 } ( %omega ) [ color red W - color blue {2 V} ]_{ m,m'} %chi_{ binom {m, m'} {n_3, n_4} } ( %omega )
-
+
+
Time-dependent
screened-exchange term
(the electron-hole interaction!)
Time-dependent Hartree term
[Speaker Notes: \mathrm{i}\frac{\partial}{\partial t}\chi^R_{\mathcal{K}\mathcal{K}^\prime} (t-t^\prime) &= \Delta E_{\mathcal{K}} \ \chi^R_{\mathcal{K}\mathcal{K}^\prime}(t-t^\prime) \\ &+\mathrm{i}\mathcal{F}_{\mathcal{K}}\left[ \delta_{\mathcal{K}\mathcal{K}^\prime} + \sum_{\overline{\mathcal{K}}} K_{\mathcal{K}\overline{\mathcal{K}}} \ \chi^R_{\overline{\mathcal{K}} \mathcal{K}^\prime}(t-t^\prime) \right]]

---
Solving the BSE for LiF
Electron-Hole Excitations in Semiconductors and Insulators
M. Rohlfing and S. G. Louie, Phys. Rev. Lett., 81, 2312 (1998)
[Speaker Notes: \textcolor{blue}{\chi_{\mathcal{K}\mathcal{K}^\prime}(\omega)} = \chi^0_{\mathcal{K}}(\omega)+  \chi^0_{\mathcal{K}}(\omega) \sum_{\overline{\mathcal{K}}} K_{\mathcal{K}\overline{\mathcal{K}}}  \ \textcolor{blue}{\chi_{\overline{\mathcal{K}} \mathcal{K}^\prime}(\omega)}]

---
Take-home message
Independent-particle picture fails to reproduce key spectral features due to lack of electron-hole interaction
The derivative of the exchange generate the electron-hole interaction and excitons
Hartree-Fock is a very bad Hamiltonian. We replace H0 with the HKS+GW and the exchange with the screened exchange
Including excitonic effects improves the agreement with experiments
[Speaker Notes: H^{2p}_{\mathcal{K}\mathcal{K}^\prime} = \Delta E_{\mathcal{K}}\delta_{ \mathcal{K} \mathcal{K}^\prime} + \mathrm{i} \mathcal{F}_{\mathcal{K}} K_{\mathcal{K}\mathcal{K}^\prime}]

---
References:
Application of the Green’s functions method to
the study of the optical properties of semiconductors
G. Strinati, La Rivista del Nuovo Cimento 11 (12), 1-86 (1980)
Effects of the Electron–Hole Interaction on the Optical Properties of Materials:
the Bethe–Salpeter Equation
G. Bussi, Phys. Scr. 2004 141 (2004)
Real-time approach to the optical properties of solids and nanostructures:
Time-dependent Bethe-Salpeter equation
C. Attaccalite, M. Grüning, and A. Marini
Phys. Rev. B 84, 245110 (2011)