Electron-Phonon coupling
a Yambo overview
ICTP Yambo school 2022
Claudio Attaccalite
CNRS/CINaM, Aix-Marseille Universite (FR)

---
Coupling electrons and phonons …
Superconductivity
Joule's heating
Electron relaxation
(luminescence)
Polaronic transport
Coherent Phonons
Peierls instability
Raman Spectroscopy
etc......

---
EPC on the electronic structure
Kink in the band structure
Temperature dependence of band gaps
A. Marini, PRL 101,106405 (2008)
Mass Enhancement

---
Energy levels renormalization
Where does the coupling come from?
Thermal expansion
Electron-Phonon interaction
>>
P.B. Allen and M. Cardona Phys. Rev. B 27 4760 (1983)

---
The quasi-harmonic approximation
Thermal expansion
It can be easily calculated using DFT and finite-differences
Grüneisen
parameters

---
A perturbative approach:
Heine-Allen-Cardona
V_scf(x+u) = V_scf(x) " " + " " {partial V_scf} over {partial x}" " u " " +" " {1} over {2} " " {partial^2 V_scf} over {partial x^2} " " u^2 " " + ....
color red {H(R + u)}= H(R) " " + " " {partial V_scf} over {partial R} " " u " " + " " {1} over {2} " " {partial^2 V_scf} over {partial R^2} " " u^2 " " + ...
Electron-phonon interactions from first principles
F. Giustino, Rev. Mod. Phys. 89, 015003 (2017)
[Speaker Notes: H e' quella elettronica della DFT. Fermiarmi al 2 ordine → expansione armonica significa assumere che le frquenze fononiche non dipendono dal volume del cristallo, quindi non sto tenendo conto di effetti anarmonici che sono legati all'expansione termica.]

---
A perturbative approach:
Heine-Allen-Cardona
V_scf(x+u) = V_scf(x) " " + " " {partial V_scf} over {partial x}" " u " " +" " {1} over {2} " " {partial^2 V_scf} over {partial x^2} " " u^2 " " + ....
color red {H(R + u)}= H(R) " " + " " {partial V_scf} over {partial R} " " u " " + " " {1} over {2} " " {partial^2 V_scf} over {partial R^2} " " u^2 " " + ...
Using KS basis and phonon eigenvectors and eigenvalues we can rewrite the perturbation as
u_{%alpha p} = left ( {M_0 over {N_p M_k} } right )^{ 1/2} sum_{ bold q %nu} e^{ i bold q bold R } e_{k %alpha,%nu } ( bold q ) l_{ bold q %nu } ( {hat a}_{bold q %nu} + {hat %alpha}^{{} +{} }_{-bold q %nu} )
The standard electron-phonon Hamiltonian
{hat H}_{ ep } = 1 over { N_p^{1/2} } sum_{ {bold k, bold q,m,n, %nu} } g_{m,n, %nu} ( bold k, bold q ) {hat c}^{ {} + {} }_{m,bold k + bold q} {hat c}_{ n, bold k } left ( {hat a}_{ bold q %nu} + {hat a}^{ {} + {} }_{- bold q %nu} right )
Electron-phonon interactions from first principles
F. Giustino, Rev. Mod. Phys. 89, 015003 (2017)
[Speaker Notes: H e' quella elettronica della DFT. Fermiarmi al 2 ordine → expansione armonica significa assumere che le frquenze fononiche non dipendono dal volume del cristallo, quindi non sto tenendo conto di effetti anarmonici che sono legati all'expansione termica.]

---
Connection with DFTP
DFPT is composed by a self-consistent linear system
El-Ph matrix elements
Dynamical Matrix
%omega_{q %lambda}
g^{q %lambda}_{nn'k} sim (M %omega_{q%lambda})^{-1} langle n k mline {d V_{KS}} over {d u_{q %lambda}} mline n'k-q rangle
[Speaker Notes: H e' quella elettronica della DFT. Fermiarmi al 2 ordine → expansione armonica significa assumere che le frquenze fononiche non dipendono dal volume del cristallo, quindi non sto tenendo conto di effetti anarmonici che sono legati all'expansione termica.]

---
Connection with DFTP
DFPT is composed by a self-consistent linear system
El-Ph matrix elements
Dynamical Matrix
%omega_{q %lambda}
g^{q %lambda}_{nn'k} sim (M %omega_{q%lambda})^{-1} langle n k mline {d V_{KS}} over {d u_{q %lambda}} mline n'k-q rangle
All matrix elements can be obtained from DFT + DFTP !!
{hat H}_{ ep } = 1 over { N_p^{1/2} } sum_{ {bold k, bold q,m,n, %nu} } g_{m,n, %nu} ( bold k, bold q ) {hat c}^{ {} + {} }_{m,bold k + bold q} {hat c}_{ n, bold k } left ( {hat a}_{ bold q %nu} + {hat a}^{ {} + {} }_{- bold q %nu} right )
Electrons
and
phonons
{hat H}_{ p } = sum_{ {bold q,%nu} } %omega_{bold q, %nu} left ( {hat a}^{ {} + {} }_{ bold q %nu} {hat a}_{ bold q %nu} + 1/2 right )
{hat H}_{ e } = sum_{ {bold k,m} } %epsilon_{bold k, m} {hat c}^{ {} + {} }_{bold k m} {hat c}_{ bold k m}
[Speaker Notes: H e' quella elettronica della DFT. Fermiarmi al 2 ordine → expansione armonica significa assumere che le frquenze fononiche non dipendono dal volume del cristallo, quindi non sto tenendo conto di effetti anarmonici che sono legati all'expansione termica.]

---
A perturbative approach:
Heine-Allen-Cardona
V_scf(R+u) = V_scf(R) " " + " " {partial V_scf} over {partial R}" " u " " +" " {1} over {2} " " {partial^2 V_scf} over {partial R^2} " " u^2 " " + ....
First order
Second order
color red {H(R + u)}= H(R) " " + " " {partial V_scf} over {partial R} " " u " " + " " {1} over {2} " " {partial^2 V_scf} over {partial R^2} " " u^2 " " + ...
For a review see M. Cardona,
Solid State Commun. 133, 3 (2005).
[Speaker Notes: H e' quella elettronica della DFT. Fermiarmi al 2 ordine → expansione armonica significa assumere che le frquenze fononiche non dipendono dal volume del cristallo, quindi non sto tenendo conto di effetti anarmonici che sono legati all'expansione termica.]

---
A perturbative approach:
Heine-Allen-Cardona
V_scf(x+u) = V_scf(x) " " + " " {partial V_scf} over {partial x}" " u " " +" " {1} over {2} " " {partial^2 V_scf} over {partial x^2} " " u^2 " " + ....
First order
Second order
color red {H(R + u)}= H(R) " " + " " {partial V_scf} over {partial R} " " u " " + " " {1} over {2} " " {partial^2 V_scf} over {partial R^2} " " u^2 " " + ...
Using Perturbation Theory, we get the correction
to the energy levels
color green {%delta E_i } = langle %PSI_i^(0) mline " " mline %PSI_i^(0) rangle " " + " " langle %PSI_i^(0) mline " " mline %PSI_i^(1) rangle " " + " " langle %PSI_i^(0) mline " " mline %PSI_i^(0) rangle " " + + ...
For a review see M. Cardona,
Solid State Commun. 133, 3 (2005).
[Speaker Notes: H e' quella elettronica della DFT. Fermiarmi al 2 ordine → expansione armonica significa assumere che le frquenze fononiche non dipendono dal volume del cristallo, quindi non sto tenendo conto di effetti anarmonici che sono legati all'expansione termica.]

---
Approximated Debye-Waller
Calculation of second derivatives
of Vscf is complicated
langle n bold k abs { {partial^2 V_scf} over {partial R_s partial R_{s'} } } n bold k rangle = 0
if s neq s'
Diagonal approximation
for the Debye-Waller

---
Approximated Debye-Waller
Calculation of second derivatives
of Vscf is complicated
langle n bold k abs { {partial^2 V_scf} over {partial R_s partial R_{s'} } } n bold k rangle = 0
Diagonal approximation
for the Debye-Waller
if s neq s'
We use the translation in-variance
%DELTA E_{n bold k} ( R_0+%DELTA R ) = %DELTA E_{n bold k} ( R_0)
{partial^2 V_scf} over {partial R^2}
{partial V_scf} over {partial R}
We get a relation between
and

---
Approximated Debye-Waller
Calculation of second derivatives
of Vscf is complicated
langle n bold k abs { {partial^2 V_scf} over {partial R_s partial R_{s'} } } n bold k rangle = 0
Diagonal approximation
for the Debye-Waller
if s neq s'
We use the translation in-variance
%DELTA E_{n bold k} ( R_0+%DELTA R ) = %DELTA E_{n bold k} ( R_0)
{partial^2 V_scf} over {partial R^2}
{partial V_scf} over {partial R}
We get a relation between
and
And we get an expression like:
langle n bold k abs { {partial^2 V_scf} over {partial R_s^2} } n bold k rangle = - sum_{ n'} {{%LAMBDA^{bold q %lambda}_{n n' bold k}} over {E_{n bold k} - E_{n' bold k}} }
g^{bold q %lambda}_{n n' bold k}
%LAMBDA^{bold q %lambda}_{n n' bold k}
where
a function of
Temperature dependence of electronic eigenenergies in the adiabatic harmonic approximation
S. Poncé, et al. Phys. Rev. B 90, 214304(2017)

---
A perturbative approach:
Heine-Allen-Cardona
%delta E_{i} (%beta) " " = " " [ {1} over {2} " " langle {partial^2 V_{scf} } over {partial R^2} rangle " " + " " Sum_{j} (E_{i} - E_{j})^{-1} langle {partial V_{scf} } over {partial R} mline j rangle langle j mline {partial V_{scf}} over {partial R} rangle ]" " langle u^2 rangle
Debye-Waller
 Average on the
electronic
wavefunction
Thermal average
Fan

---
A perturbative approach:
Heine-Allen-Cardona
%delta E_{i} (%beta) " " = " " [ {1} over {2} " " langle {partial^2 V_{scf} } over {partial R^2} rangle " " + " " Sum_{j} (E_{i} - E_{j})^{-1} langle {partial V_{scf} } over {partial R} mline j rangle langle j mline {partial V_{scf}} over {partial R} rangle ]" " langle u^2 rangle
Debye-Waller
 Average on the
electronic
wavefunction
Thermal average
FINAL FORMULA
%delta E_{n bold k} (%beta) = Sum_{bold q %lambda n'} [ {lline g^{bold q %lambda}_{n n' bold k} rline} over {E_{n bold k} - E_{n' bold k +bold q} } -{%LAMBDA^{bold q %lambda}_{n n' bold k}} over {E_{n bold k} - E_{n' bold k}} ](2 B(%omega_{bold q %lambda}) +1)
Fan
Clear dependence on the
Temperature
B(wq) = Bose function

---
It's time to revise previous electronic structure calculations?

---
The gap of diamond
Electronic Gap: 7.715 eV
Renormalization: 615 meV
F. Giustino, et al. PRL, 105, 265501 (2010)
E. Cannuccia, Phys. Rev. Lett. 107, 255501 (2011)
Logothedis et al. PRB 46, 4483 (1992)
The e-h interaction
Is not taken into account,
It does not modify qualitatively
the line shape of the absorption
edge
Classical ions
[Speaker Notes: C, N, O .. have no p-electrons in the core and the p valence electrons, as the atoms vibrate, can get much closer to the core than in cases where p-electrons are present in the core: germanium, silicon, GaAs….]

---
Beyond the static perturbation theory
All the previous theory can be reformulated in term of Green's function including non-adiabatic effects
Electron-phonon interactions from first principles
Feliciano Giustino
Rev. Mod. Phys. 89, 015003 (2017)
FAN
[Speaker Notes: Cambio di base: cartesiane → fonone displacement k-q]

---
Electron-phonon coupling from
a MBPT perspective
Electron-Phonon Self Energy
Temperature dependence
%epsilon_{n bold {k}} E_{n bold k}(T)+i %GAMMA_{n bold k}(T)
Electron scatters with 1 phonon at a time
E_{nk} %GAMMA_{nk}
Spectral Functions
[Speaker Notes: Cambio di base: cartesiane → fonone displacement k-q]

---
Quasi-particle band structure
Temperature dependence of electronic eigenenergies in the adiabatic harmonic approximation
S. Poncé, et al. Phys. Rev. B 90, 214304 (2014)

---
Quasi-particle band structure
Temperature dependence of electronic eigenenergies in the adiabatic harmonic approximation
S. Poncé, et al. Phys. Rev. B 90, 214304 (2014)

---
Dynamical effects in diamond
Signature of the dynamical effects
E. Cannuccia, Phys. Rev. Lett. 107, 255501 (2011)
Logothedis et al. PRB 46, 4483 (1992)
%GAMMA

---
Optical properties at finite temperature
H^{el}_{K,K'}=(%epsilon_e-%epsilon_h)%delta_{K,K'}
=
Quasihole and quasielectron
{tilde L}_{K_1,K_2}(%tau)={tilde L}^{(0)}_{K_1,K_2}(%tau)[%delta_{2,3}+%PI^{el}_{K_2,K_3}(%tau=0)]{tilde L}_{K_3,K_2}(%tau)
tilde{L}
The excitons are the poles of
and eigenstates of the
Bethe-Salpeter Hamiltonian
%epsilon_2(%omega) = sum_{%lambda}{ {{abs{D}_{%lambda}}^2 } over {%omega-%epsilon_{%lambda} + i %eta} }

---
Optical properties at finite temperature
We can include in L0 corrections derived from electron-phonon coupling by replacing:
=
Quasihole and quasielectron
{tilde L}_{K_1,K_2}(%tau)={tilde L}^{(0)}_{K_1,K_2}(%tau)[%delta_{2,3}+%PI^{el}_{K_2,K_3}(%tau=0)]{tilde L}_{K_3,K_2}(%tau)
%epsilon_{n bold {k}} E_{n bold k}(T)+i %GAMMA_{n bold k}(T)

---
Optical properties at finite temperature
We can include in L0 corrections derived from electron-phonon coupling by replacing:
The bare electron-hole Hamiltonian at finite T become:
H^{0}_{K,K'}(T)=[E_e(T)-E_h(T)]%delta_{K,K'} + i[ %GAMMA_e(T) - %GAMMA_h(T)] %delta_{K,K'}
The final BSE amiltonian is NOT Hermitian anymore
=
Quasihole and quasielectron
{tilde L}_{K_1,K_2}(%tau)={tilde L}^{(0)}_{K_1,K_2}(%tau)[%delta_{2,3}+%PI^{el}_{K_2,K_3}(%tau=0)]{tilde L}_{K_3,K_2}(%tau)
%epsilon_{n bold {k}} E_{n bold k}(T)+i %GAMMA_{n bold k}(T)

---
Optical properties at finite temperature
We have a BSE at finite temperature
=
Quasihole and quasielectron

---
Optical properties at finite temperature
We have a BSE at finite temperature
Dielectric constant at finite T
Exciton non-radiative lifetime
%tau_{%lambda}(T) = 1 over {2 Im [E_{%lambda}(T)] }
=
Quasihole and quasielectron
%epsilon_2(%omega,T) = sum_{%lambda}{ {{abs{D}_{%lambda}}^2 } over {%omega-E_{%lambda}(T) } }

---
Optical properties at finite temperature
Finite temperature excitons
Andre Marini, PRL 101, 106405 (2008)

---
Optical properties at finite temperature
Finite temperature excitons
Andre Marini, PRL 101, 106405 (2008)
This method fails for too strong bond excitons
Lowest exciton should have zero life-time
Theory of exciton-phonon coupling
G. Antonius and S. G. Louie Phys. Rev. B 105, 085111(2022)
Exciton-Phonon Interaction and Relaxation Times from First Principles
H. Chen, D. Sangalli, and M. Bernardi PRL. 125, 107401(2020)

---
Yambo implementation 1/3

---
Yambo implementation 2/3
Double-grid method
replace:
with:
D. Kammerlander, et al. Phys. Rev. B 86, 125203(2012)
E. Cannuccia, C. Attaccalite and V. Olevano ...to be published soon

---
Yambo implementation 3/3

---
Yambo implementation
H. Kawai et al.
Phys. Rev. B 89, 085202 (2014)
E. Cannuccia and A. Marini,
Phys. Rev. Lett. 107, 255501 (2011)
Finite temperature excitons
A. Marini, PRL 101, 106405 (2008)
References:
Electron-phonon interactions
from first principles
Feliciano Giustino
Rev. Mod. Phys. 89, 015003 (2017)
Theory of exciton-phonon coupling
G. Antonius and S. G. Louie
Phys. Rev. B 105, 085111(2022)
Temperature dependence of electronic eigenenergies in the adiabatic harmonic approximation
S. Poncé, et al. Phys. Rev. B 90, 214304 (2014)
M. Cardona,
Solid State Commun. 133, 3 (2005).