A squashed and squeezed h-BN
Claudio Attaccalite
L. Artús, A. Segura.
M. Feneberg, J. H. Edgar, J. Li, R. Goldhahn, T. Taniguchi, K. Watanabe, R. Cuscó,
F. Paleari, P. Lechifflart

---
Optical spectra of h-BN 1/2
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC
Luis Artús, M. Feneberg, C. Attaccalite, J. H. Edgar, J. Li, R. Goldhahn, Ramon Cuscó
Advanced Photonics Research 2 (5), 2000101(2021)

---
Optical spectra of h-BN 2/2
Two-photon absorption in two-dimensional materials: The case of h-BN
C. Attaccalite, M. Grüning, H. Amara, S. Latil, and F. Ducastelle Phys. Rev. B 98, 165126 (2018)
Excitons in few-layer hexagonal boron nitride: Davydov splitting and surface localization
F. Paleari et al. 2D Mater. 5 045017 (2018)

---
Optical spectra of h-BN 2/2
Davydov splitting
Two-photon absorption in two-dimensional materials: The case of h-BN
C. Attaccalite, M. Grüning, H. Amara, S. Latil, and F. Ducastelle Phys. Rev. B 98, 165126 (2018)
Excitons in few-layer hexagonal boron nitride: Davydov splitting and surface localization
F. Paleari et al. 2D Mater. 5 045017 (2018)

---
hBN at finite pressure
Sapphire anvils
These are not trivial experiments, as conventional diamond anvil cells cannot be used to optically access the bandgap spectral range of h-BN. Instead, one has to use
sapphire anvils, which are rather brittle and prone to crack easily under pressure.

---
Reflectance spectra of h-BN
under pressure

---
h-BN under pressure: atomic structure

---
hBN under pressure: the band structure
A Unified Understanding of the Thickness-Dependent Bandgap Transition in Hexagonal Two-Dimensional Semiconductors
Kang, J.; Zhang, L.; Wei, S.-H. , J. Phys. Chem. Lett. 2016, 7, 597−602 (2016)

---
hBN under pressure: excitons
Excitons decomposition
Gaps and excitons
under pressure

---
hBN under pressure: excitons
 Exciton binding energies
as a function of pressure
Gaps and excitons
under pressure

---
Experiments vs theory
Direct and indirect excitonic transitions determined from the reflectance spectra compared with the ab-initio theoretical calculations (solid lines).

---
h-BN under strain

---
Band structure under uni-axial stress
Direct band-gap
Indirect band-gap

---
Excitons under strain 1/2
Exciton positions follow the gaps

---
Excitons under strain 2/2
Exciton positions follow the gaps
Breaking of 120º rotation!!

---
Luminescence

---
Experiments
Vibrational Properties in Highly Strained Hexagonal Boron Nitride Bubbles
Elena Blundo et al.
Nano Lett. , 22, 4, 1525–1533 (2022)
[Up to 2.5% strain!!!]
h-BN on micro-structures substrate
Léonard Schué, J. Barjon, A. Loiseau
work in progress

---
Conclusions
Ellipsometric study performed with synchrotron radiation in 2D/layered compounds up to 25 eV
We have investigated the pressure-induced shifts of direct and indirect excitonics in bulk h-BN layered crystal, reduction exciton binding energy.
Uniaxial strain effect on optical proprties of h-BN, breaking the symmetries
References
Ellipsometry Study of Hexagonal Boron Nitride Using Synchrotron Radiation: Transparency Window in the Far‐UVC
Luis Artús, M. Feneberg, C. Attaccalite, J. H. Edgar, J. Li, R. Goldhahn, Ramon Cuscó
Advanced Photonics Research 2 (5), 2000101(2021)
Tuning the Direct and Indirect Excitonic Transitions of h‐BN by Hydrostatic Pressure
A. Segura, R. Cuscó, C. Attaccalite, T. Taniguchi, K. Watanabe, and L. Artús,
The Journal of Physical Chemistry C 125 (23), 12880-12885 (2021)
Excitons under strain: light absorption and emission in strained hexagonal boron nitride
P. Lechifflart, F. Paleari, C. Attaccalite, SciPost Phys. 12, 145 (2022)

---
Reflectivity and reflectance
Calculated reflectivity spectrum associated with the direct excitonic transitions (dashed line), compared with the experimental reflectance measurement (red dots). The blue and green sigmoidal dotted lines account for, respectively, the drop of reflectance due to the absorption at the direct and indirect excitonic energies suppressing the reflection at the bottom interface. The solid line is the resulting calculated reflectance after taking into account the self-absorption effect.

---
hBN is one of the
preferred materials by theoreticians
2D exciton dispersion
Exciton-phonon coupling
Tight-binding
F. Paleari et al 2018 2D Mater. 5 045017
L. Sponza et al. Phys. Rev. B 98, 125206(2018)
F. Paleari et al PRL. 122, 187401 (2019)
E. Cannuccia et al. PRB 99, 081109(R)(2019)
P. Cudazzo PRL 116, 066803 (2016)
J. Koskelo et al. PRB 95, 035125 (2017)
Exictons in
non-linear response
Benchmark
for total energy
2D phonon dispersion
T. Sohier et al. NanoLetters 17, 3758 (2017)
C. Attaccalite et al. PRB 98 165126 (2018)
T. G. Pedersen, PRB 92, 235432 (2015)
T.Gruber et al. PRX 8, 021043 (2018)

---
Ellipsometry Study of Hexagonal Boron Nitride using Synchrotron Radiation

---
Theory vs experiments 1/2
….perfect agreement?...
Electron-phonon	DGap
PRB 99, 165201 (2019)	0.273 eV
PRB 101, 205115 (2020)	0.35 eV (0.4 at 300K)
PRB 102, 045117 (2020)	0.2 eV
	First Exciton
Exp.	6.12 eV
GoWo + BSE	5.76 eV
evGW + BSE	6.03 eV
QSGW + BSE PRM 2, 034603 (2018)	6.11 eV
Reduction exciton binding energy PRL 101,106405 (2008)	30% * 0.8eV = 0.26 eV
and more: vertex correction, phonon screening